__________________________________________________________________________________________________________

PART 1 - GENERAL

1.1	SUMMARY

- Scope of work - Provide ceramic tile, tile installation materials and accessories as indicated on drawings, as specified herein, and as needed for complete and proper installation.

- Related Documents - provisions within General and Supplementary General Conditions of the Contract, Division 1 - General Requirements, and the Drawings apply to this Section.

1.2	SECTION INCLUDES

- Ceramic wall tile and trim units (glazed)

- Ceramic floor tile/mosaics and trim units (glazed or unglazed)

- Ceramic tile pavers and trim units (glazed or unglazed)

- Quarry tile pavers and trim units (glazed or unglazed)

- Porcelain tile

- Glass tile (including mosaics)

- Special purpose tile

- Decorative thin wall tile

- Installation Products; adhesives, mortars, grouts and sealants

- Waterproofing membranes for ceramic tile work

- Anti-fracture membranes for ceramic tile work

- Sound control underlayments

- Thresholds, trim, cementitious backer units and other accessories specified herein.

NOTE TO SPECIFIER: Edit for applicable procedures & materials

1.3	PRODUCTS FURNISHED BUT NOT INSTALLED UNDER THIS SECTION

NOTE TO SPECIFIER: Edit for applicable products

1.4	PRODUCTS INSTALLED BUT NOT FURNISHED UNDER THIS SECTION

NOTE TO SPECIFIER: Edit for applicable products

1.5	ENVIRONMENTAL PERFORMANCE REQUIREMENTS

A.	Environmental Performance Criteria:  The following criteria are required for products included in this section.

Refer to Division 1 for additional requirements:

1.

2.    Adhesive products must meet or exceed the VOC limits of South Coast Air Quality Management District

(SCAQMD) Rule #1168 and Bay Area Air Quality Management District (BAAQMD) Reg. 8, Rule 51.

1.6	RELATED SECTIONS

- Section 03 30 00 Cast-in-Place Concrete (monolithic slab finishing for ceramic tile)

- Section 03 30 00 Concrete Curing

- Section 03 40 00 Structural Pre-cast Concrete

- Section 03 53 00 Concrete Floor Topping

- Section 04 20 00 Unit Masonry (CMU wall substrates)

- Section 04 40 00 Stone Assemblies

- Section 06 10 00 Rough Carpentry (plywood sub-floors)

- Section 07 13 00 Dampproofing and Waterproofing

- Section 07 92 00 Joint Sealants

- Section 09 29 00 Gypsum Board Assemblies

- Section 09 30 00 Tiling

- Section 09 30 33 Stone Tile

- Section 10 28 00 Toilet, Bath and Laundry Accessories

- Section 22 40 00 Plumbing Fixtures

NOTE TO SPECIFIER: Above are examples of typical broad scope and narrow scope sections related to ceramic tile installation. Edit for applicable related sections

1.7	ALLOWANCES

NOTE TO SPECIFIER: Edit for detail of applicable ALLOWANCES; coordinate with Section 01020 Allowances.  Allowances in the form of unit pricing are sometimes used when the scope of the tile work at time of bid is undetermined.

1.8	ALTERNATES

NOTE TO SPECIFIER: Edit for applicable ALTERNATES.  Alternates may be used to evaluate varying levels of performance of setting systems or to assist in the selection of the tile by economy.

1.9	REFERENCE STANDARDS

- American Iron and Steel Institute (AISI) Specification for the Design of Cold-Formed Steel Structural Members

- American National Standards Institute (ANSI) A137.1 American National Standard Specifications For Ceramic Tile

- American National Standards Institute (ANSI) A137.2 American National Standard Specifications For Glass Tile

- American National Standards Institute (ANSI) A137.3 American National Standard Specifications For Gauged Porcelain Tile and Gauged Porcelain Tile Panels/Slabs

- American National Standards Institute (ANSI) A108.01 - A108.21 American National Standard Specifications For The Installation Of Ceramic Tile

- American National Standards Institute (ANSI) A118.1 - A118.19 American National Standard Specifications For The Installation Of Ceramic Tile

- American National Standards Institute (ANSI) A136.1 American National Standard Specifications For The Installation Of Ceramic Tile

- American Plywood Association (APA) Y510T Plywood Design Specifications

- American Society For Testing And Materials (ASTM) A82 Standard Specification for Steel Wire, Plain, for Concrete Reinforcement

- American Society For Testing And Materials (ASTM) A185 Standard Specification for Steel Welded Wire Fabric, Plain, for Concrete Reinforcement

- American Society For Testing And Materials (ASTM) C33 Standard Specification for Concrete Aggregate

- American Society For Testing And Materials (ASTM) C36 Standard Specification for Gypsum Wallboard

- American Society For Testing And Materials (ASTM) C109 Standard Test Method for Compressive Strength of Hydraulic Cement Mortars (Using 2-in. or 50-mm Cube Specimens)

- American Society For Testing And Materials (ASTM) C144 Standard Specification for Aggregate for Masonry Mortar

- American Society For Testing And Materials (ASTM) C150 Standard Specification for Portland Cement

- American Society For Testing And Materials (ASTM) C171 Standard Specification for Sheet Materials for Curing Concrete

- American Society For Testing And Materials (ASTM) C241 Standard Test Method for Abrasion Resistance of Stone Subjected to Foot Traffic

- American Society For Testing And Materials (ASTM) C267 Standard Test Method for Chemical Resistance of Mortars, Grouts, and Monolithic Surfacings

- American Society For Testing And Materials (ASTM) C482 Standard Test Method for Bond Strength of Ceramic Tile to Portland Cement

- American Society For Testing And Materials (ASTM) C503 Standard Specification for Marble Dimension Stone (Exterior)

- American Society For Testing And Materials (ASTM) C531 Standard Test Method for Linear Shrinkage and Coefficient of Thermal Expansion of Chemical-Resistant Mortars, Grouts, Monolithic Surfacings and Polymer Concretes

- American Society For Testing And Materials (ASTM) C627 Standard Test Method for Evaluating Ceramic Floor Tile Installation Systems Using the Robinson-Type Floor Tester

- American Society For Testing And Materials (ASTM) C794 Standard Test Method for Adhesion-in-Peel of Elastomeric Joint Sealants

- American Society For Testing And Materials (ASTM) C847 Standard Specification for Metal Lath

- American Society For Testing And Materials (ASTM) C905 Standard Test Method for Apparent Density of Chemical-Resistant Mortars, Grouts, and Monolithic Surfacings

- American Society For Testing And Materials (ASTM) C920 Standard Specification for Elastomeric Joint Sealants

- American Society For Testing And Materials (ASTM) C955 Standard Specification for Load Bearing (Transverse and Axial) Steel Studs, Runners (Tracks), and Bracing or Bridging for Screw Application of Gypsum Board and Metal Plaster Bases

- American Society For Testing And Materials (ASTM) D226 Standard Specification for Asphalt-Saturated Organic Felt Used in Roofing And Waterproofing

- American Society For Testing And Materials (ASTM) D227 Standard Specification for Coal-Tar Saturated Organic Felt Used in Roofing and Waterproofing

- American Society For Testing And Materials (ASTM) D751 Standard Test Method for Coated Fabrics

- American Society For Testing And Materials (ASTM) D1037 Standard Test Methods for Evaluating Properties of Wood-Base Fiber and Particle Panel Materials

- American Society For Testing And Materials (ASTM) D1248 Standard Test Method for Staining of Porous Substances by Joint Sealants

- American Society For Testing And Materials (ASTM) D1621 Standard Test Method for Compressive Properties of Rigid Cellular Plastics

- American Society For Testing And Materials (ASTM) D2240 Standard Test Method for Rubber Property – Durometer Hardness

- American Society For Testing And Materials (ASTM) D4263 Standard Test Method for Indicating Moisture in Concrete by The Plastic Sheet Method

- American Society For Testing And Materials (ASTM) D4397 Standard Specification for Polyethylene Sheeting for Construction, Industrial and Agricultural Applications

- American Society For Testing And Materials (ASTM) D4716 Standard Test Method for Determining the (In Plane) Flow Rate Per Unit Width and Hydraulic Transmissivity of a Geo-synthetic Using a Constant Head

- American Society For Testing And Materials (ASTM) E84 Standard Test Method for Surface Burning Characteristics of Building Materials

- American Society For Testing And Materials (ASTM) E90 Standard Test Method for Laboratory Measurement of Airborne Sound Transmission Loss of Building Partitions

- American Society For Testing And Materials (ASTM) E96 Standard Test Methods for Water Vapor Transmission of Materials

- American Society For Testing And Materials (ASTM) E413 Standard Classification for Rating Sound Insulation

- American Society For Testing And Materials (ASTM) E492 Standard Test Method for Laboratory Measurement of Impact Sound Transmission Through Floor-Ceiling Assemblies Using the Tapping Machine

- American Society For Testing And Materials (ASTM) E989 Standard Classification for Determination of Impact Insulation Class (IIC)

- American Society For Testing And Materials (ASTM) E1155 Standard Test Method for Determining FF Floor Flatness and FL Floor Levelness

- American Society For Testing And Materials (ASTM) F710 Standard Practice for Preparing Concrete Floors to Receive Resilient Flooring

- American Society For Testing And Materials (ASTM) F1869 Standard Test Method for Measuring Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride

- American Society For Testing And Materials (ASTM) F2170 Standard Test Method for Determining Relative Humidity in Concrete Floor Slabs Using in-situ Probes

- American Society of Mechanical Engineers (ASME) - ASME A112.6.3 Floor and Trench Drains

- Canadian Sheet Steel Building Institute (CSSBI) Lightweight Steel Framing Binder {Publication 52M}

- Federal Housing Administration (FHA) Bulletin No. 750 Impact Noise Control in Multifamily Dwellings

- Housing and Urban Development (HUD) TS 28 A Guide to Airborne, Impact and Structure-borne Noise-Control in Multifamily Dwellings

- International Organization for Standardization (ISO) 13007 Standards for Grouts and Adhesives

- Materials And Methods Standards Association (MMSA) Bulletins 1-16

- Metal Lath/Steel Framing Association (ML/SFA) 540 Lightweight Steel Framing Systems Manual

- Steel Stud Manufacturers Association (SSMA) Product Technical Information and ICBO Evaluation Service, Inc. Report ER-4943P

- Terrazzo, Tile And Marble Association Of Canada (TTMAC) Specification Guide 09300 Tile Installation Manual

- Tile Council Of North America (TCNA) Handbook For Ceramic, Glass, and Stone Tile Installation

NOTE TO SPECIFIER: edit for applicable reference standards

1.10	SYSTEM DESCRIPTION

- Ceramic mosaic floor tile installed over concrete floor slabs using latex-modified portland cement mortar and latex portland cement grout joints.

- Quarry tile and base installed using latex modified portland cement mortar over a plastic portland cement mortar bed or over a cured (pre-floated) portland cement mortar bed with epoxy grouted joints.

NOTE TO SPECIFIER: The above systems are example descriptions; edit for additional applicable systems

  - SUBMITTALS

NOTE TO SPECIFIER: Edit for applicable requirements

- Submittal Requirements: Submit the following “Required LEED Criteria” certification items as listed below.  Refer to Division 1 for additional requirements:

  - A completed LEED Environmental Building Materials Certification Form.  Information to be

supplied generally includes:

    - Manufacturing plant locations for tile installation products.

    - LEED Credits as listed in Part 1.4B “LEED Credit Submittals”

    - Recycled content; pre-consumer or post-consumer; or;

Project specific information gathered using the LATICRETE LEED Project Certification Assistant available at https://laticrete.com/en/innovation-and-impact/green-leed/leed-project-certification-assistant.

  - UL GREENGUARD Certification Program For Chemical Emissions For Building Materials, Finishes

And Furnishings, UL 2818 or UL GREENGUARD Gold certificates provided by the tile installation materials manufacturer on UL GREENGUARD letterhead stating “This product has been UL GREENGUARD Gold Product Certified For Low Chemical Emissions by the UL Environment under the UL GREENGUARD Certification Program For Chemical Emissions For Building Materials, Finishes And Furnishings” for each tile installation product used to verify Low VOC product information.

  - Contractor’s certification of LEED Compliance: Submit Contractor’s certification verifying the

installation of specified LEED Compliant products.

  - Product Cut Sheets for all materials that meet the LEED performance criteria.  Submit Product Cut

Sheets with Contractor or Sub-contractor’s stamp, as confirmation that submitted products were

installed on Project.

  - Safety Data Sheets for all applicable products.

- LEED Credit Submittals for the following;

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit Building

Product Disclosure and Optimization – Environmental Product Declarations: Manufacturer’s Product

Specific (Type III) Environmental Product Declarations for LATICRETE Cement Mortar for Tile

Installation, LATICRETE Cement Grout for Tile Installation, and/or LATICRETE Cement Self-Leveling

Underlayment.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit Building

Product Disclosure and Optimization – Material Ingredients: Manufacturer’s product data for tile

installation materials, including Health Product Declaration (HPD) on HPD Collaborative letterhead.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit Building

Product Disclosure and Optimization – Sourcing of Raw Materials Option 2 (Recycled Content):

Manufacturer’s product data for tile installation materials.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit:

Building Product Disclosure and Optimization – Sourcing of Raw Materials Option 2 (Regional

Materials): Product data indicating location of material manufacturer for regionally manufactured

Materials (within 100 miles of project site).

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 Edition MR Credit Construction and Demolition Waste Management: Path 1 (Divert 50% and Three Material Streams) Manufacturer’s packaging showing recycle symbol for appropriate disposition in construction waste management.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 Edition MR Credit Construction and Demolition Waste Management: Path 1 (Divert 75% and Four Material Streams) Manufacturer’s packaging showing recycle symbol for appropriate disposition in construction waste management.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 EQ Credit

Low-Emitting Materials: Manufacturer’s product data for tile installation materials, including UL

GREENGUARD Gold Certificate on UL GREENGUARD letterhead stating product VOC emissions.

8.   LEED Schools Reference Guide (Educational Projects Only), 2007 Edition Credit EQ 9 (Enhanced

Acoustical Performance): Impact noise reduction test reports and product data on sound control

product(s).

9.   LEED Schools Reference Guide (Educational Projects Only), 2007 Edition Credit EQ 10 (Mold

Prevention): Manufacturer’s packaging and/or data showing anti-microbial protection in product(s).

- Submit shop drawings and manufacturers' product data under provisions of Section (01 30 00)

(01 34 00)

- Submit samples of each type/style/finish/size/color of ceramic tile, mosaic, paver, trim unit or threshold under provisions of Section (01 30 00)  (01 34 00)

- Submit manufacturers' installation instructions under provisions of Section (01 30 00)  (01 34 00)

- Submit manufacturer's certification under provisions of Section (01405) that the materials supplied conform to ANSI A137.1 for ceramic tile or ANSI A137.2 for glass tile.

- Submit proof of warranty.

- Submit Health Product Declarations (HPD) for each tile installation material.

I.    Submit Product Specific (Type III) for Environmental Product Declarations for Cement Mortars for Tile

Installation, Cement Grouts for Tile Installation, and/or Cement Self-Leveling Underlayments specified.

- Submit sample of installation system demonstrating compatibility/functional relationships between adhesives, mortars, grouts and other components under provision of Section (01 30 00) (01 34 00).  Submit proof from tile or stone manufacturer or supplier verifying suitability of tile or stone for specific application and use; including dimensional stability, water absorption, freeze/thaw resistance (if applicable), resistance to thermal cycling, and other characteristics that the may project may require. These characteristics must be reviewed and approved by the project design professional(s).

- Submit list from manufacturer of installation system/adhesive/mortar/grout identifying a minimum of three (3) similar projects, each with a minimum of three (3) years service.

- For alternate materials, at least thirty (30) days before bid date submit independent laboratory test results confirming compliance with specifications listed in Part 2 - Products.

1.12	QUALITY ASSURANCE

NOTE TO SPECIFIER: Edit for applicable requirements

It is strongly recommended to use installers who have demonstrated a commitment to their craft and taken the time to stay current with the latest materials and methods. Requiring references and a portfolio along with a bid or estimate is a good way to ensure the installer has successfully completed work of similar size, scope, and complexity. Pools, exterior facades, mortar beds, shower pans, steam showers, etc. require different skills. Matching installer ability to the project at hand requires close evaluation of their experience, training, state licensing (where applicable), and certifications/credentials (where applicable). The Ceramic Tile Education Foundation (CTEF) provides a Contractor Questionnaire that can be used to aid in evaluating and comparing contractors (www.tilecareer.com).

Various programs administered by associations, non-profit educational organizations, unions, and private companies serve the tile industry by providing education, hands-on training, and evaluation of the skills and competency of installers and contractors. It is important to distinguish between the many programs available:

- Hands-on training

- Evaluation/certification of installation skills

- On-line training

- On-line knowledge evaluation (without a hands-on component)

As with all programs, the rigor and credibility of the program must also be considered.

The following non-profit programs are well-established and recognized by the Tile Council of North America’s (TCNA) Handbook Committee (listed alphabetically):

Ceramic Tile Education Foundation (CTEF) Certified Tile Installer Program: CTEF tests hands-on installation skills and knowledge. Installers must achieve the minimum required score on both tests to earn the “CTEF Certified Installer” designation. Contractors that employ CTEF Certified Installers are listed in the CTEF Contractor Directory, in the TCNA Handbook for Ceramic, Glass and Stone Tile and on the CTEF website. See www.tilecareer.org for more information.

International Masonry Institute (IMI) Contractor College Program: IMI conducts professional and technical courses for union masonry and tile contractors, which lead to certification in installation and project supervision. See www.imiweb.org for more information.

Journeyman Tile Layer Apprenticeship Programs: Installers recognized by the U.S. Department of Labor (DOL) as Journeyman Tile Layers are required to fulfill and document several years of training and on-the-job experience as apprentices to become Journeymen. The majority of these setters earn their Journeyman status through union-affiliated training programs, although some non-union tile contractors administer their own DOL-recognized apprenticeship programs and employ journeyman tile layers. Contractors that employ union Journeyman Tile Setters can be found through the union locals that list their signatory contractors, primarily the Bricklayer and Allied Craftworkers (BAC) and the United Brotherhood of Carpenters (UBC). See www.bacweb.org and www.carpenters.org for more information.

National Tile Contractors Association (NTCA) Five Star Contractor Program: NTCA is a tile contractors association, with membership open to all tile contractors. Their Five Star program is a peer review program to recognize NTCA members who have demonstrated a track record of providing successful installations. Earning the Five Star designation requires recommendations from customers, suppliers, and peers as well as participation in continuing education, training, and safety programs. See www.tile-assn.com for more information.

Tile Contractors’ Association of America (TCAA) Trowel of Excellence Program: TCAA is a contractors association for BAC signatory contractors. Its Trowel of Excellence program is a peer review program to recognize TCAA members who have demonstrated a track record of providing successful installations. Earning the Trowel of Excellence designation requires letters of reference, submittal of a detailed project description and photos, employee participation in educational programming, and proof of financial responsibility. See www.tcaainc.org for more information.

- Tile Manufacturer (single source responsibility): Company specializing in ceramic tile, mosaics, pavers, trim units and/or thresholds with three (3) years minimum experience.  Obtain tile from a single source with resources to provide products of consistent quality in appearance and physical properties.

- Installation System Manufacturer (single source responsibility): Company specializing in adhesives, mortars, grouts and other installation materials with ten (10) years minimum experience and ISO 9001-2008 certification.  Obtain installation materials from single source manufacturer to insure consistent quality and full compatibility.

- Submit laboratory confirmation of adhesives, mortars, grouts and other installation materials:

  - Identify proper usage of specified materials using positive analytical method.

  - Identify compatibility of specified materials using positive analytical method.

  - Identify proper color matching of specified materials using a positive analytical method.

- Installer qualifications: company specializing in installation of ceramic tile, mosaics, pavers, trim units and thresholds with five (5) years documented experience with installations of similar scope, materials and design.

1.13	MOCK-UPS

- Provide mock-up of each type/style/finish/size/color of ceramic tile, mosaics, pavers, trim unit and threshold, along with respective installation adhesives, mortars, grouts and other installation materials, under provisions of Section (01400) (01405).

1.14	PRE-INSTALLATION CONFERENCE

Pre-installation conference: At least three weeks prior to commencing the work attend a meeting at the jobsite to discuss conformance with requirements of specification and job site conditions.  Representatives of owner, architect, general contractor, tile subcontractor, Tile Manufacturer, Installation System Manufacturer and any other parties who are involved in the scope of this installation must attend the meeting.

1.15	DELIVERY, STORAGE AND HANDLING

- Acceptance at Site: deliver and store packaged materials in original containers with seals unbroken and labels, including grade seal, intact until time of use, in accordance with manufacturer's instructions.

- Store ceramic tile and installation system materials in a dry location; handle in a manner to prevent chipping, breakage, and contamination.

- Protect latex additives, organic adhesives, epoxy adhesives and sealants from freezing or overheating in accordance with manufacturer's instructions; store at room temperature when possible.

- Store portland cement mortars and grouts in a dry location.

1.16	PROJECT/SITE CONDITIONS

- Provide ventilation and protection of environment as recommended by manufacturer.

- Prevent carbon dioxide damage to ceramic tile, mosaics, pavers, trim, thresholds, as well as adhesives, mortars, grouts and other installation materials, by venting temporary heaters to the exterior.

C.   Maintain ambient temperatures not less than 50ºF (10ºC) or more than 100ºF (38ºC) during installation and for a minimum of seven (7) days after completion.  Setting of portland cement is retarded by low

temperatures.  Protect work for extended period of time and from damage by other trades.  Installation with latex portland cement mortars requires substrate, ambient and material temperatures at least 37ºF (3ºC).  There should be no ice in slab.  Freezing after installation will not damage latex portland cement mortars. Protect portland cement based mortars and grouts from direct sunlight, radiant heat, forced ventilation (heat & cold) and drafts until cured to prevent premature evaporation of moisture. Epoxy mortars and grouts require surface temperatures between 60ºF (16ºC) and 90ºF (32ºC) at time of installation. It is the General Contractor’s responsibility to maintain temperature control.

1.17	SEQUENCING AND SCHEDULING

- Coordinate installation of tile work with related work.

- Proceed with tile work only after curbs, vents, drains, piping, and other projections through substrate have been installed and when substrate construction and framing of openings have been completed.

NOTES FOR SPECIFIER:  Edit for project specific sequence and scheduling

1.18      WARRANTY

The manufacturer of adhesives, mortars, grouts and other installation materials shall provide a written twenty five (25) year warranty, which covers materials and labor - reference LATICRETE Warranty Data Sheet 025.0 for complete details and requirements.  For exterior facades over steel or wood framing, the manufacturer of adhesives, mortars, grouts and other installation materials shall provide a written fifteen (15) year warranty, which covers replacement of LATICRETE products only – reference LATICRETE Warranty Data Sheet 230.15 for complete details and requirements.

1.19	MAINTENANCE

Submit maintenance data under provisions of Section 01 73 00. Include cleaning methods, cleaning solutions recommended, stain removal methods, as well as polishes and waxes recommended.

1.20	EXTRA MATERIALS STOCK

Upon completion of the work of this Section, deliver to the Owner 2% minimum additional tile and trim shape of each type, color, pattern and size used in the Work, as well as extra stock of adhesives, mortars, grouts and other installation materials for the Owner's use in replacement and maintenance. Extra stock is to be from same production run or batch as original tile and installation materials.

PART 2 - PRODUCTS

2.1	TILE MANUFACTURERS

Subject to compliance with paragraphs 1.12 and performance requirements, provide products by one of the following manufacturers:

NOTE TO SPECIFIER: Provide list of acceptable tile manufacturers.

2.2	WALL TILE MATERIALS

NOTE TO SPECIFIER: edit for each tile type

- Ceramic Tile:

- Grade:

- Size:

- Edge:

- Finish:

- Color:

- Special shapes:

- Location:

2.3	FLOOR TILE MATERIALS

NOTE TO SPECIFIER: edit for each tile type

- Ceramic Tile:

- Grade:

- Size:

- Edge:

- Finish:

- Color:

- Special shapes:

- Location:

2.4	CERAMIC TILE INSTALLATION MATERIALS MANUFACTURER

- LATICRETE International, Inc., 1 Laticrete Park North, Bethany, CT 06524-3423 USA Phone 800-243-4788, (203) 393-0010 technicalservices@laticrete.com;  https://laticrete.com;  https://laticrete.com/en/innovation-and-impact/green-leed

NOTE TO SPECIFIER: Use either the following performance specification or the proprietary specification.

2.5	PERFORMANCE SPECIFICATION - TILE INSTALLATION ACCESSORIES

- Waterproofing Membrane to be thin, cold applied, single component liquid and load bearing. Reinforcing fabric to be non-woven rot-proof specifically intended for waterproofing membrane.  Waterproofing Membrane to be non-toxic, non-flammable and non-hazardous during storage, mixing, application and when cured. It shall be certified by IAPMO and ICC approved as a shower pan liner and shall also meet the following physical requirements:

  - Hydrostatic Test (ASTM D4068):              	     Pass

  - Elongation @ break (ASTM D751):	20-30%

  - System Crack Resistance (ANSI A118.12):	Pass (High)

  - 7 day Tensile Strength (ANSI A118.10):                      >265 psi (1.8 MPa)

  - 7 day Shear Bond Strength (ANSI A118.10)               >200 psi (1.4 MPa)

  - 28 Day Shear Bond Strength (ANSI A118.4):	>214 psi (1.48 – 2.4 MPa)

  - Service Rating (TCA/ASTM C627): 	Extra Heavy

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

B.    Epoxy Waterproofing Membrane to be 3 component epoxy, trowel applied specifically designed to be used under ceramic tile, stone, masonry veneer, or brick and requires only 24 hours prior to flood testing:

  - Breaking Strength (ANSI A118.10):              	     450-530 psi (3.1-3.6 MPa)

  - Waterproofness (ANSI A118.10):	No Water penetration

  - 7 day Shear Bond Strength (ANSI A118.10):              110-150 psi (0.8-1 MPa)

  - 28 Day Shear Bond Strength (ANSI A118.10):	90-120 psi (0.6–0.83 MPa)

  - 12 Week Shear Bond Strength (ANSI A118.10):        110-130 psi (0.8-0.9 MPa)

  - Total VOC Content:                                                     <3.4 g/L

C.   Crack Suppression Membrane to be thin, cold applied, single component liquid and load bearing.  Reinforcing fabric (if required or used) to be non-woven, rot-proof specifically intended for crack suppression membrane.  Materials to be non-toxic, non-flammable, and non-hazardous during storage, mixing, application and when cured. Crack Suppression Membrane shall also meet the following physical requirements:

  - Elongation @ break (ASTM D751):	20-30%

  - System Crack Resistance (ANSI A118.12)	Pass (High)

  - 7 day Tensile Strength (ANSI A118.10):                      265 – 300 psi (1.8 – 2.0 MPa)

  - 7 day Shear Bond Strength (ANSI A118.10):              200 – 275 psi (1.4 – 1.9 MPa)

  - 28 Day Shear Bond Strength (ANSI A118.4):	>214 – 343 psi (1.48 – 2.4 MPa)

  - Service Rating (TCA/ASTM C627): 	Extra Heavy

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

D.  Wire Reinforcing:  2 inch x 2 inch (50 x 50 mm) x 16 ASW gauge or 0.0625 inch (1.6mm) diameter

galvanized steel welded wire mesh complying with ANSI A108.02 3.7, ASTM A185 and ASTM A82.

E.  Cleavage membrane: 15 pound asphalt saturated, non-perforated roofing felt complying with ASTM  D226, 15 pound coal tar saturated, non-perforated roofing felt complying with ASTM D227 or 4.0 mils (0.1 mm) thick polyethylene plastic film complying with ASTM D4397.

F.   Cementitious backer board units: size and thickness as specified, complying with ANSI A118.9.

G.   Thresholds:  Provide marble saddles complying with ASTM C241 for abrasion resistance and ASTM

C503 for exterior use, in color, size, shape and thickness as indicated on drawings.

NOTE TO SPECIFIER:  Edit applicable tile installation accessories.

PERFORMANCE SPECIFICATION - TILE INSTALLATION MATERIALS

- Tile Board shall be high density, waterproof extruded polystyrene core with a reinforced, waterproof membrane on both sides.  Board to be available in multiple thicknesses and suitable for use on interior walls, floors, ceilings, shower/tub surrounds, and steam rooms, as well as meet the following physical requirements:

  - Water Vapor Transmission (ASTM E96 Method E):   0.034 Perms

  - Compressive Strength (ASTM D1621):                       >55 psi (0.38 MPa)

  - Flexural Strength (IAPMO Z124):	Pass

4.    Linear Expansion (ASTM D1037):	-0.04%

- Sound Abatement & Crack Isolation Mat shall be load bearing, shock and vibration resistant.  It shall be certified by independent laboratory testing to meet the specified acoustical performance when installed in a Floor Assembly with a 6" (150mm) concrete slab, as well as meet the following physical requirements:

  - Service Rating (ASTM C627):                                     Moderate

  - Installed Weight (ASTM C905 Modified):	4.3 lbs./ft2 (21.1 kg/m2)

  - Delta Impact Insulation Class (ΔIIC; ASTM E2179):	22

- Sound Abatement & Crack Suppression Adhesive shall comply with ANSI A118.12, provide an Extra Heavy rating, UL GREENGUARD Gold compliant, and provide a minimum ΔIIC of 15:

1.   Service Rating (ASTM C627):                   	Extra Heavy

2.   Delta Impact Insulation Class (ΔIIC; ASTM E2179):    15

3.   Point Load (ANSI A118.12 5.2):                                   >1,000 psi (6.9 MPa)

4.   Minimum Shear Bond Strength (ANSI A118.12):         100psi (0.7 MPa)

- Uncoupling Membrane shall comply with ANSI A118.12, provide an Extra Heavy rating and allow for use with ANSI A118.4 thin-bed mortars:

1.   Service Rating (ASTM C627):	Extra Heavy

2.   System Crack Resistance (ANSI A118.12 5.4):	Pass (High)

3.   Point Load (ANSI A118.12 5.2):	Pass

- Moisture Vapor Reduction to be epoxy based and UL GREENGUARD Gold compliant as well as meet the following physical requirements:

1.    Shear Bond to Concrete (ANSI A118.12-5.1.5):          >285 psi (2.0 MPa)

2.    Alkalinity Resistance (ASTM C267):                            Pass

3.    Permeability (ASTM F1869):                                        9.7 lbs/1,000ft2/24 hours down to 0.2

lbs/1,000 ft2/24hours (248 µg/s•m2 down to

11 µg/s•m2)

4.   Total VOC Emissions:	 ≤0.22 mg/m3

- Latex Portland Cement Mortar for thick beds, screeds, leveling beds and scratch/plaster coats to be weather, frost, shock resistant, UL GREENGUARD Gold compliant, and meet the following physical requirements:

  - Compressive Strength (ANSI A118.4 Modified):         >4,000 psi (27.6 MPa)

  - Water Absorption (ANSI A118.6):	≤ 5%

  - Service Rating (TCA/ASTM C627):                             Extra Heavy

  - Smoke & Flame Contribution (ASTM E84 Modified):  0

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Self-Leveling Underlayment shall be mixed with water to produce a pumpable, fast setting, free flowing cementitious underlayment which can be poured from 1/8” to 1 ¼” (3 - 32mm) thick in one pour.

  - Flexural Strength (ASTM C1708):	            >840 psi (5.8 MPa)

  - 28 Day Compressive Strength (ANSI A118.4 Mod.):  >4,000 psi (27.6 MPa)

  - Tensile Strength (ANSI A118.7):                                 >270 psi (1.9 MPa)

  - Time To Foot Traffic @ 70˚F (21˚C):                          1 – 4 Hours

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Epoxy Adhesive to be chemical resistant 100% solids epoxy with high temperature resistance, UL GREENGUARD Gold compliant, conform to ISO R2, and meet the following minimum physical requirements:

  - Compressive strength (ANSI A118.3):	>5,000 psi (34.4 MPa)

  - Shear Bond Strength (ANSI A118.3):	>1,250 psi (8.6 MPa)

  - Thermal Shock Resistance (ANSI A118.3):                >600 psi (4.1 MPa)

  - Tensile Strength (ANSI A118.3):                                 >1,400 psi (9.6 MPa)

  - Shrinkage (ANSI A118.3):                                           0 – 0.1%

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

  - Cured Epoxy Adhesive to be chemically and stain resistant to ketchup, mustard, tea, coffee, milk, soda, beer, wine, bleach (5% solution), ammonia, juices, vegetable oil, detergents, brine, sugar, cosmetics and blood, as well as chemically resistant to dilute food acids, dilute alkalis, gasoline, turpentine and mineral spirits.

- Latex Portland Cement Thin Bed Mortar for thin set and slurry bond coats to be weather, frost, shock resistant, non-flammable, UL GREENGUARD Gold compliant, conform to ISO C2TES1 and meet the following physical requirements:

  - Tensile adhesion strength (ISO 13007-2 4.4.2):	>260 psi (1.8 MPa)

  - 28 day shear bond strength (ANSI A118.15):	>475 psi (3.3 MPa)

  - 7 day water immersion shear (ANSI A118.15):	>250 psi (1.7 MPa)

  - Smoke & Flame Contribution (ASTM E84 Modified):  0

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Latex Portland Cement Large, Heavy Tile Mortar for thin set and slurry bond coats to be weather, frost, shock resistant, non-flammable, UL GREENGUARD Gold compliant, and meet the following physical requirements:

  - 28 Day shear bond strength (ANSI A118.15):	≥500 psi (3.45 MPa)

  - 28 Day Freeze/Thaw Cycling (ANSI A118.15):	≥400 psi (2.76 MPa)

  - 7 day water immersion shear (ANSI A118.15):           ≥350 psi (2.4 MPa)

  - Sag Resistance (ANSI A118.15):                                0 mm

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Organic Adhesive shall be a non-flammable, water resistant, latex adhesive and shall meet the following physical requirements:

  - Open Time (ANSI A136.1):	70 minutes @ 75°F (24°C)

  - Color:	White

  - Density (ANSI A136.1):	13.2 lbs/gal (1.6 kg/l)

  - Total VOC Content	<36.00 g/L

- Epoxy Grout (Industrial) to be non-flammable, chemical resistant 100% solids epoxy with high temperature resistance, UL GREENGUARD Gold compliant,  and meeting the following physical requirements:

  - Initial Set Time (ANSI A118.5):	Pass (4 hours)

  - Service Set Time (ANSI A118.5):	Pass (< 7 days)

  - Shrinkage (ANSI A118.3):	0.07%

  - Sag (ANSI A118.3):	Pass (No sag)

  - Shear Bond Strength (ANSI A118.3; quarry tile):	2,200 psi (15.2 MPa)

  - Compressive Strength (ANSI A118.3):	8,300 psi (57.2 MPa)

  - Tensile Strength (ANSI A118.5):	3,000 psi (20.7 MPa)

  - Thermal Shock Resistance (ANSI A118.3):	2,100 psi (14.5 MPa)

  - Total VOC Emissions:	≤0.22 mg/m3

  - Cured Epoxy Grout to be chemically and stain resistant to ketchup, mustard, tea, coffee, milk, soda, beer, wine, bleach (3% solution), ammonia, juices, vegetable oil, detergents, brine, sugar, cosmetics, and blood, as well as being chemically resistant to dilute food/mineral acids, gasoline and mineral spirits.

- Epoxy Grout (Commercial/Residential) shall be non-toxic, non-flammable, non-hazardous during storage, mixing, application and  when cured, UL GREENGUARD Gold compliant,  and shall meet the following physical requirements:

  - Compressive Strength (ANSI A118.3):                                3,800 psi (26.2 MPa)

  - Shear Bond Strength (ANSI A118.3):                                  1,100 psi (7.6 MPa)

  - Tensile Strength (ANSI A118.3):                                         1,100 psi (7.6 MPa)

  - Thermal Shock (ANSI A118.3):                                            >800 psi (5.5 MPa)

  - Water Absorption (ANSI A118.3):                                        <0.05%

  - Vertical Joint Sag (ANSI A118.3):                                        Pass

  - Total VOC Emissions:                                                          ≤0.22 mg/m3

  - Cured Epoxy Grout to be chemically and stain resistant to ketchup, mustard, tea, coffee, milk, soda, beer, wine, bleach (5% solution), ammonia, juices, vegetable oil, brine, sugar, cosmetics, and blood, as well as chemically resistant to dilute acids and dilute alkalis.

- Latex Portland Cement Grout to be weather, frost and shock resistant, UL GREENGUARD Gold compliant, as well as meet the following physical requirements:

  - Compressive Strength (ANSI A118.7):	 4,500 psi (31 MPa)

  - Tensile Strength (ANSI A118.7):                                  500 psi (3.4 MPa)

  - Flexural Strength (ANSI A118.7):                                 1,250 psi (8.6 MPa)

  - Water Absorption (ANSI A118.7):	 < 5%

  - Linear Shrinkage (ANSI A118.7):                                 < 0.05 %

  - Smoke & Flame Contribution (ASTM E84 Modified):   0

  - Total VOC Emissions:                                                  ≤0.22 mg/m3

N.   Expansion and Control Joint Sealant to be a one component, neutral cure, exterior grade silicone sealant and meet the following requirements:

  - Tensile Strength (ASTM C794):	280 psi (1.9 MPa)

  - Hardness (ASTM D751; Shore A):                              25 (colored sealant) /15 (clear sealant)

  - Weather Resistance (QUV Weather-ometer):            10,000 hours (no change)

  - VOC Emissions:	≤0.5 mg/m3

  - VOC Content:	≤37.16 g/L

O.   Roof Decks (and other exterior paving applications over occupied/storage spaces) shall consist of a Primary Roofing/Waterproofing Membrane, as specified in Section 0700 (q.v.), and a lightweight, frost/weather resistant installation system for tile, pavers, brick and stone that provides integral subsurface drainage and meets the following physical requirements:

  - Compressive Strength (ASTM C109 Modified):	3,000 psi (20.7 MPa)

  - Hydraulic Transmissivity (ASTM D4716):	1.6 gal./minute (6.1 L/minute)

  - Service Rating (ASTM C627):                                      Extra Heavy

P.   Spot Bonding Epoxy Adhesive for installing tile, brick, masonry veneer, and stone over vertical and overhead surfaces shall be high strength, high temperature resistant, non-sag and shall meet the following physical requirements:

  - Thermal Shock Resistance (ANSI A118.3):	>1,000 psi (6.9 MPa)

  - Water Absorption (ANSI A118.3):                                0.1 %

  - Compressive Strength (ANSI A118.3):	>8,300 psi (57.2 MPa)

  - Shear Bond Strength (ANSI A118.3 Modified):	>730 psi (5 MPa)

Q.   Sealer shall be water-based and provide maximum protection against both water- and oil- based stains, and meet the following requirements:

1.    Surface Traffic: 6 – 8 hours

2.    Full Cure in 24 – 72 hours

3.    VOC Compliant: 12 g/L (low solids coating)

4.    Natural Look Sealer

NOTE TO SPECIFIER:  Edit applicable tile installation materials.

2.6	PROPRIETARY SPECIFICATION - TILE INSTALLATION ACCESSORIES

Installation accessories as manufactured by LATICRETE International, Inc., 1 LATICRETE Park North, Bethany, CT  06524-3423 USA. Phone 800-243-4788, www.laticrete.com

- Waterproofing Membrane: LATICRETE HYDRO BAN® ** as manufactured by LATICRETE International, Inc.

- Epoxy Waterproofing Membrane: LATAPOXY® Waterproof Flashing Mortar as manufactured by LATICRETE International, Inc.

- Crack Suppression Membrane: LATICRETE® HYDRO BAN® ** as manufactured by LATICRETE International, Inc.

NOTE TO SPECIFIER:  Edit applicable tile installation accessories.

PROPRIETARY SPECIFICATION - TILE INSTALLATION MATERIALS

Installation materials as manufactured by LATICRETE International, Inc., 1 LATICRETE Park North, Bethany, CT  06524-3423 USA. Phone 800-243-4788, www.laticrete.com; www.laticrete.com/green

- Tile Board: LATICRETE HYDRO BAN Board as manufactured for LATICRETE International, Inc.

- Sound Control Underlayment: LATICRETE 170.5 Sound & Crack Isolation Mat as manufactured for LATICRETE International, Inc.

- Sound & Crack Isolation Adhesive: LATICRETE 125 TRI MAX** as manufactured by

LATICRETE International, Inc.

C.   Uncoupling Membrane: LATICRETE STRATA_MAT™ as manufactured for LATICRETE International, Inc.

D.   Electric Radiant Floor Heat System: LATICRETE STRATA_HEATTM Mat with

LATICRETE STRATA_HEAT Spliceless Wire as manufactured for LATICRETE International, Inc.

- Moisture Vapor Reduction: LATICRETE VAPOR BAN™ E as manufactured by LATICRETE International, Inc.

- Latex-Portland Cement Mortar for thick beds, screeds, leveling beds and scratch/plaster coats: LATICRETE 3701 Fortified Mortar Bed** as manufactured by LATICRETE International, Inc.

- Self-Leveling Underlayment: LATICRETE NXT LEVEL PLUS™ as manufactured by LATICRETE International, Inc.

- Epoxy Adhesive: LATAPOXY 300 Adhesive** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Thin Bed Mortar: LATICRETE 254 PLATINUM™** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Thin Bed Mortar: LATICRETE 254 PLATINUM PLUS** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Thin Bed Mortar: LATICRETE 253 Gold** as manufactured by LATICRETE International, Inc.

- Medium Bed Mortar: LATICRETE MULTIMAX™ LITE** as manufactured by LATICRETE International, Inc.

- Organic Adhesive: LATICRETE 15 Premium Mastic as manufactured for LATICRETE International, Inc.

- Epoxy Grout (Industrial): LATICRETE SPECTRALOCK® 2000 IG** as manufactured by LATICRETE International, Inc.

- Epoxy Grout (Commercial/Residential): LATICRETE SPECTRALOCK® PRO Premium Grout** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Grout: LATICRETE PERMACOLOR® Select** as manufactured by LATICRETE International, Inc.

- Expansion and Control Joint Sealant: LATICRETE LATASIL™ ^ as manufactured for LATICRETE International, Inc.

- Roof Deck: LATICRETE Plaza & Deck System as manufactured by LATICRETE International, Inc.

- Spot Bonding Epoxy Adhesive: LATAPOXY 310 Stone Adhesive as manufactured for LATICRETE International, Inc.

- Sealer: STONETECH BulletProof® Sealer as manufactured for LATICRETE International, Inc.

**   UL GREENGUARD Certified For Low Chemical Emissions (ULCOM/GG 2818) and UL GREENGUARD Gold Certified For Low Chemical Emissions (ULCOM/GG UL 2818)

^     Independently tested per CDPH v1.2 for Low VOC Emissions to meet ≤0.5mg /m3.

END OF SECTION

©2024 LATICRETE International, Inc., all rights reserved

IT IS NOT THE INTENT OF THIS GUIDE TO MAKE MOVEMENT JOINT RECOMMENDATIONS FOR A SPECIFIC PROJECT.

Architect or engineer must specify movement joints and show location and details on drawings.

Perimeter and field movement joints within a tile or stone installation are essential and required.

Note: Preparation of openings left by the tile contractor and installation of backup strip and sealant should be specified in the Caulking and Sealant section of the job specification.

The performance requirements of certain special locations, such as swimming pools, dairies, food plants, etc., may exceed the minimum requirements of the sealant specifications given above. Therefore, follow recommendations of experienced manufacturers as to specific sealants suitable for the job environment. In some severe environments, a program for regular maintenance of sealant in joints may be required.

Provide control or expansion joints as located in contract drawings and in full conformity, especially in width and depth, with architectural details.

- Substrate joints must carry through, full width, to surface of tile, brick, masonry veneer, or stone.

- Install expansion joints in tile, brick, masonry veneer, or stone work over construction/cold joints or control joints in substrates.

- Install expansion joints where tile, brick, masonry veneer, or stone abut restraining surfaces (such as perimeter walls, curbs and columns), changes in plane and corners.

- Optimum ratio of joint length: joint width is 1:1 and must not exceed 2:1. Sealant joint width: joint depth should be ~ 2:1.

- Joint width and spacing depends on application – follow Tile Council of North America “Handbook for Ceramic, Glass, and Stone Tile Installation” Detail “EJ-171 Expansion Joints” guidelines or consult sealant manufacturer for recommendation based on project parameters.

- Joint width must be ≥ 1/8” (3mm) and ≤ 1” (25mm).

Location and Frequency of Movement Joints:

• Interior – 20’ to 25’ (6.1 – 7.6m) in each direction.

• Exterior – 8’ to 12’ (2.4 – 3.7m) in each direction.

• Interior tile work exposed to direct sunlight or moisture – 8’ to 12’ (2.4 – 3.7m) in each direction.

• Above-ground concrete slab structure – 8’ to 12’ (2.4 – 3.7m) in each direction.

• Perimeter Joints – movement joints are required where tile work abuts restraining surfaces such as perimeter walls, dissimilar floors, curbs, columns, pipes, ceilings, and where changes occur in backing materials.

• All expansion, control, construction, cold, and seismic joints in the structure should continue through the tile work, including such joints at vertical surfaces.

• Joints through tile work directly over structural joints must never be narrower than the structural joint.

• Where tile pattern falls diagonally across a saw-cut joint, relocation of the movement joint is specifically not recommended because of the reduced performance of the sealant when used in a saw tooth or other non-linear fashion.  Tile to be cut to continue from the diagonal saw cut joint directly up through the tile work.

Expansion Joint Width (Vertical & Horizontal):

• Exterior (all tile) – minimum 3/8” (10mm) for joints 8’ (2.4m) on center, minimum ½” (12mm) for joints 12’ (3.7m) on center. Minimum widths must be increased 1/16” (1.5mm) for each 15°F (8°C) tile surface temperature change greater than 100°F (38°C) between summer high and winter low. (Decks exposed to the sky in northern U.S.A. usually require ¾” (19mm) wide joints on 12’ (3.7m) centers.

• Interior for quarry tile and paver tile – same as grout joints, but not less than ¼” (6mm).

• Interior for ceramic mosaic tile and glazed wall tile – preferred not less than ¼” (6mm), but never less than 1/8” (3mm).

• Joints in tile and setting materials shall never be less than the width of the saw-cut control joint width.

• Joints through tile work directly over structural joints must never be narrower than the structural joint.

Preparation:

Remove all contaminants and foreign material from joint spaces/surfaces, such as dirt, dust, oil, water, frost, setting/grouting materials, sealers, and old sealant/backer. Use LATICRETE® LATASIL™ 9118 Primer for underwater and permanent wet area applications, or, for installations of porous stone (e.g. limestone, sandstone etc…).  Install appropriate backing material (e.g. closed cell backer rod) based on expansion joint design and as specified in §07 92 00. Apply masking tape to face of tile, brick or stone veneer.  Use a caulking gun, or other applicator, to fill joints with sealant.  Within 5-10 minutes of filling joint, ‘tool’ sealant surface to a smooth finish. Remove masking tape immediately after tooling joint.  Wipe smears or excess sealant off the face of non-glazed tile, brick, stone or other absorptive surfaces immediately.

Materials:

Backup strip shall be a flexible and compressible type of closed-cell foam polyethylene, butyl rubber, or open cell and closed cell polyurethane, rounded at surface to contact sealant as recommended by sealant manufacturers. It must fit neatly into the joint without compacting and to such a height to allow a sealant depth of ½ the width of the joint. Sealant must not bond to the backup material. Silicone sealants contain plasticizers that may stain some natural stones.  Conduct a test area under actual site conditions to determine suitability and acceptability of sealant with the stone chosen for the project.

Cold Joints:

• Cold joints are formed primarily between slab pours where the size of a concrete slab may be too large to be poured at one time. The remainder of the slab would be poured on a later date, forming a cold joint between the two sections. Such joints should be shown on architectural drawings.

• A cold joint becomes a weakened joint that, upon movement, will crack, permitting leakage or buckling and cracking of a tile floor set over the slab.

Control Joints:

• Formed, sawed or tooled groove in a concrete structure to create a weakened plane and regulate the location of cracking resulting from the dimensional change of different parts of the structure.

• Also referred to a saw-cut joint.

Expansion Joints:

• A separation provided between adjoining parts of a structure to allow movement where expansion is likely to exceed contraction

• A separation between pavement slabs on grade, filled with a compressible filler material

• An isolation joint intended to allow independent movement between adjoining parts

Isolation Joints:

• A separation between adjoining parts of a concrete structure, usually a vertical plane, at a designated location such as to interfere least with performance of the structure.

• To allow relative movement in three directions and avoid formation of cracks elsewhere in the concrete and through which all or part of the bonded reinforcement is interrupted.

Some large slabs on-grade are poured monolithically, then later saw-cut at intervals, providing control/contraction joints to allow for cracking at these weakened points.

Installation:

• Movement joints in tile should be located over all cold joints and saw-cut control joints.

• Joints in tile and setting materials shall never be less than the width of the saw-cut control joint width. Preparation and installation shall be as required for movement joints.

• To ensure that location of joints in tile work align with existing joints in substrate, joints in tile work should be constructed during installation of mortar beds and/or tile, rather than saw-cutting joints after installation.

• Keep movement joint cavities open and free of direct, debris, grout, mortar, and setting materials.

• Tile edges to which the sealant will bond must be clean and dry.

• Some sealants require edge priming. Consult primer sealant manufacturer’s specifications for proper parameters for primer use. If required, care must be taken to keep primer off tile/stone face.

• Set compressible backup strip when mortar is placed or utilize removable wood strip to provide space for backup after mortar has cured.

• Install sealant after tile work and grout are dry. Follow sealant manufacturer’s recommendations.

• Refer to movement joint section in ANSI tile installation specifications.

Use the following LATICRETE System Materials:
LATICRETE® LATASIL™

LATICRETE LATASIL 9118 Primer

References:

LATICRETE Data Sheets: 6200.1,  6528.1

LATICRETE SDS: LATASIL, Primer

LATICRETE Detail Drawings: WP300, WP301, WP302, WP303, EJ-01, EJ-02, EJ-03, EJ-04, EJ-05, EJ-06, EJ-07, EJ-08, EJ-09, EJ-10, EJ-11, EJ-12, EJ-13, EJ-14, EJ-15 (Sealant treatments only for specific types of movement joints)

LATICRETE Technical Data Sheets: 211, 251, 252

EJ-01 – Typical Expansion Joint - Thick Bed Unbonded

EJ-02 – Typical Expansion Joint - Thick Bed Bonded

EJ-03 – Typical Isolation/Expansion Joint - Thin Bed

EJ-04 – Typical Control Joint - Thin Bed

EJ-05 – Typical Perimeter Joint - Thin Bed

EJ-06 – Typical Generic Movement Joint

EJ-07 – Typical Expansion Joint - Thin Bed

EJ-08 – Expansion Joint with Waterproofing Membrane Below Thick Bed

EJ-09 – Control Joint with Anti-Fracture Membrane

EJ-10 – Expansion Joint with Waterproofing Membrane Above Thick Bed

EJ-11 – Expansion Joint - Thin Bed with Waterproofing Membrane

EJ-12 – Floor at Bathtub Waterproofing Membrane

EJ-13 – Interior Floor - Marble Threshold with Waterproofing Membrane

EJ-14 – Cold Joint

EJ-15 – Movement Joint - Unbonded Thick Bed with Waterproofing Membrane

Metal Edge Trim LATICRETE Profiles & Trims fulfill a wide range of needs including edge protection, floor transitions, decorative and more. Installed indoors and outdoors, they can be used with multiple floor coverings such as tile and stone, terrazzo, wood and LVT. Create unique designs with a selection of finishes and colors in kitchens and bathrooms, commercial and residential applications, and everything in between.

Application:

    - Select the correct size of profile according to the tile thickness.

    - Prior to installing the tile, make sure the profiles, corners, and connectors are accurately measured and dry-fitted. Measure and mark the profile to the correct length before cutting.

    - Apply tile adhesive with a margin or notched trowel to the area where the profile will be installed.

    - Firmly press the profile into the adhesive, allowing the adhesive to flow through octagonal cutouts in the mounting leg.

    - Adjust and straighten the profile if necessary. Using an appropriate notched trowel and adhesive for the tile to be installed, add more adhesive over the mounting leg and surface fully embedding the mounting leg of the profile.

    - Press the tile firmly into the adhesive to achieve full coverage, ensuring the profile and tile are aligned and flush. Leave a 1/16" to 1/8" gap between the profile and tile for grouting.

    - Continue tiling the rest of the area. Immediately after installing the profiles and tile, clean the surface of the profile to remove any residual adhesive or cement material with clean fresh water and a sponge or microfiber cloth.

Use the following LATICRETE System Materials:

LATICRETE Profiles & Trims

References:

Ej-171 And All Floor and Wall Methods: Ej-171 And All Floor and Wall Methods

“As a professional courtesy, LATICRETE offers technical services free of charge. The user maintains all responsibility for verifying the applicability and suitability of the technical service or information provided."

The right to copy, distribute and utilize for commercial purposes is granted exclusively to architects, engineers, and specification writers.  Execution Statements are subject to change without notice.  For latest revision, check our website @ https://laticrete.com

ES-EJ171        R  01 April 2024

All references are the intellectual property of their respective owners:

TCNA Handbook for Ceramic, Glass, and Stone Tile Installation. Tile Council of North America, Inc. Anderson, SC, 2021.

American National Standard Specifications for Installation of Ceramic Tile. Tile Council of North America, Inc. Anderson, SC, 2021.

Annual Book of ASTM Standards. American Society for Testing and Materials. West Conshohocken, PA, 2001.

American National Standard Specifications for Ceramic Tile (ANSI A137.1). Tile Council of North America, Inc. Anderson, SC 2021.

American National Standard Specifications for Glass Tile (ANSI A137.2). Tile Council of North America, Inc. Anderson, SC, 2019.

American National Standard Specifications for Gauged Porcelain Tile and Gauged Porcelain Tile Panels/Slabs (ANSI A137.3). Tile Council of North America, Inc. Anderson, SC, 2020.

ISO 13007 Ceramic Tiles – Grouts and Adhesives, International Organization for Standardization (ISO), Geneva, Switzerland, 2004.

Floor and Trench Drains - ASME A112.6.3. American Society of Mechanical Engineers. New York, NY, 2001 (R 2007).

International Building Code, International Code Council. Country Club Hills, IL, 2018.

International Residential Code for One- and Two-Family Dwellings, International Code Council. Country Club Hills, IL, 2018.

LEED Reference Guide for Green Building Design and Construction v4. U.S Green Building Council. Washington, D.C., 2013.

LEED Schools Reference Guide. U.S. Green Building Council. Washington D.C., 2007.

Lightweight Steel Framing Design Manual. Canadian Sheet Steel Building Institute. Cambridge, ON, Canada, 2006.

North American Specification for the Design of Cold-Formed Steel Structural Members. American Iron and Steel Institute. Washington D.C., 2007.

ICBO ER-4943P Product Technical Information. Steel Stud Manufacturers Association. Chicago, IL, 2001.

Lightweight Steel Framing Systems Manual. Metal Lath/Steel Framing Association Division. Glen Ellyn, IL.