__________________________________________________________________________________________________________

PART 1 - GENERAL

1.1	SUMMARY

- Scope of work - Provide ceramic tile, tile installation materials and accessories as indicated on drawings, as specified herein, and as needed for complete and proper installation.

- Related Documents - provisions within General and Supplementary General Conditions of the Contract, Division 1 - General Requirements, and the Drawings apply to this Section.

1.2	SECTION INCLUDES

- Ceramic wall tile and trim units (glazed)

- Ceramic floor tile/mosaics and trim units (glazed or unglazed)

- Ceramic tile pavers and trim units (glazed or unglazed)

- Quarry tile pavers and trim units (glazed or unglazed)

- Porcelain tile

- Glass tile (including mosaics)

- Special purpose tile

- Decorative thin wall tile

- Installation Products; adhesives, mortars, grouts and sealants

- Waterproofing membranes for ceramic tile work

- Anti-fracture membranes for ceramic tile work

- Sound control underlayments

- Thresholds, trim, cementitious backer units and other accessories specified herein.

NOTE TO SPECIFIER: Edit for applicable procedures & materials

1.3	PRODUCTS FURNISHED BUT NOT INSTALLED UNDER THIS SECTION

NOTE TO SPECIFIER: Edit for applicable products

1.4	PRODUCTS INSTALLED BUT NOT FURNISHED UNDER THIS SECTION

NOTE TO SPECIFIER: Edit for applicable products

1.5	ENVIRONMENTAL PERFORMANCE REQUIREMENTS

A.	Environmental Performance Criteria:  The following criteria are required for products included in this section.

Refer to Division 1 for additional requirements:

1.

2.    Adhesive products must meet or exceed the VOC limits of South Coast Air Quality Management District

(SCAQMD) Rule #1168 and Bay Area Air Quality Management District (BAAQMD) Reg. 8, Rule 51.

1.6	RELATED SECTIONS

- Section 03 30 00 Cast-in-Place Concrete (monolithic slab finishing for ceramic tile)

- Section 03 30 00 Concrete Curing

- Section 03 40 00 Structural Pre-cast Concrete

- Section 03 53 00 Concrete Floor Topping

- Section 04 20 00 Unit Masonry (CMU wall substrates)

- Section 04 40 00 Stone Assemblies

- Section 06 10 00 Rough Carpentry (plywood sub-floors)

- Section 07 13 00 Dampproofing and Waterproofing

- Section 07 92 00 Joint Sealants

- Section 09 29 00 Gypsum Board Assemblies

- Section 09 30 00 Tiling

- Section 09 30 33 Stone Tile

- Section 10 28 00 Toilet, Bath and Laundry Accessories

- Section 22 40 00 Plumbing Fixtures

NOTE TO SPECIFIER: Above are examples of typical broad scope and narrow scope sections related to ceramic tile installation. Edit for applicable related sections

1.7	ALLOWANCES

NOTE TO SPECIFIER: Edit for detail of applicable ALLOWANCES; coordinate with Section 01020 Allowances.  Allowances in the form of unit pricing are sometimes used when the scope of the tile work at time of bid is undetermined.

1.8	ALTERNATES

NOTE TO SPECIFIER: Edit for applicable ALTERNATES.  Alternates may be used to evaluate varying levels of performance of setting systems or to assist in the selection of the tile by economy.

1.9	REFERENCE STANDARDS

- American Iron and Steel Institute (AISI) Specification for the Design of Cold-Formed Steel Structural Members

- American National Standards Institute (ANSI) A137.1 American National Standard Specifications For Ceramic Tile

- American National Standards Institute (ANSI) A137.2 American National Standard Specifications For Glass Tile

- American National Standards Institute (ANSI) A137.3 American National Standard Specifications For Gauged Porcelain Tile and Gauged Porcelain Tile Panels/Slabs

- American National Standards Institute (ANSI) A108.01 - A108.21 American National Standard Specifications For The Installation Of Ceramic Tile

- American National Standards Institute (ANSI) A118.1 - A118.19 American National Standard Specifications For The Installation Of Ceramic Tile

- American National Standards Institute (ANSI) A136.1 American National Standard Specifications For The Installation Of Ceramic Tile

- American Plywood Association (APA) Y510T Plywood Design Specifications

- American Society For Testing And Materials (ASTM) A82 Standard Specification for Steel Wire, Plain, for Concrete Reinforcement

- American Society For Testing And Materials (ASTM) A185 Standard Specification for Steel Welded Wire Fabric, Plain, for Concrete Reinforcement

- American Society For Testing And Materials (ASTM) C33 Standard Specification for Concrete Aggregate

- American Society For Testing And Materials (ASTM) C36 Standard Specification for Gypsum Wallboard

- American Society For Testing And Materials (ASTM) C109 Standard Test Method for Compressive Strength of Hydraulic Cement Mortars (Using 2-in. or 50-mm Cube Specimens)

- American Society For Testing And Materials (ASTM) C144 Standard Specification for Aggregate for Masonry Mortar

- American Society For Testing And Materials (ASTM) C150 Standard Specification for Portland Cement

- American Society For Testing And Materials (ASTM) C171 Standard Specification for Sheet Materials for Curing Concrete

- American Society For Testing And Materials (ASTM) C241 Standard Test Method for Abrasion Resistance of Stone Subjected to Foot Traffic

- American Society For Testing And Materials (ASTM) C267 Standard Test Method for Chemical Resistance of Mortars, Grouts, and Monolithic Surfacings

- American Society For Testing And Materials (ASTM) C482 Standard Test Method for Bond Strength of Ceramic Tile to Portland Cement

- American Society For Testing And Materials (ASTM) C503 Standard Specification for Marble Dimension Stone (Exterior)

- American Society For Testing And Materials (ASTM) C531 Standard Test Method for Linear Shrinkage and Coefficient of Thermal Expansion of Chemical-Resistant Mortars, Grouts, Monolithic Surfacings and Polymer Concretes

- American Society For Testing And Materials (ASTM) C627 Standard Test Method for Evaluating Ceramic Floor Tile Installation Systems Using the Robinson-Type Floor Tester

- American Society For Testing And Materials (ASTM) C794 Standard Test Method for Adhesion-in-Peel of Elastomeric Joint Sealants

- American Society For Testing And Materials (ASTM) C847 Standard Specification for Metal Lath

- American Society For Testing And Materials (ASTM) C905 Standard Test Method for Apparent Density of Chemical-Resistant Mortars, Grouts, and Monolithic Surfacings

- American Society For Testing And Materials (ASTM) C920 Standard Specification for Elastomeric Joint Sealants

- American Society For Testing And Materials (ASTM) C955 Standard Specification for Load Bearing (Transverse and Axial) Steel Studs, Runners (Tracks), and Bracing or Bridging for Screw Application of Gypsum Board and Metal Plaster Bases

- American Society For Testing And Materials (ASTM) D226 Standard Specification for Asphalt-Saturated Organic Felt Used in Roofing And Waterproofing

- American Society For Testing And Materials (ASTM) D227 Standard Specification for Coal-Tar Saturated Organic Felt Used in Roofing and Waterproofing

- American Society For Testing And Materials (ASTM) D751 Standard Test Method for Coated Fabrics

- American Society For Testing And Materials (ASTM) D1037 Standard Test Methods for Evaluating Properties of Wood-Base Fiber and Particle Panel Materials

- American Society For Testing And Materials (ASTM) D1248 Standard Test Method for Staining of Porous Substances by Joint Sealants

- American Society For Testing And Materials (ASTM) D1621 Standard Test Method for Compressive Properties of Rigid Cellular Plastics

- American Society For Testing And Materials (ASTM) D2240 Standard Test Method for Rubber Property – Durometer Hardness

- American Society For Testing And Materials (ASTM) D4263 Standard Test Method for Indicating Moisture in Concrete by The Plastic Sheet Method

- American Society For Testing And Materials (ASTM) D4397 Standard Specification for Polyethylene Sheeting for Construction, Industrial and Agricultural Applications

- American Society For Testing And Materials (ASTM) D4716 Standard Test Method for Determining the (In Plane) Flow Rate Per Unit Width and Hydraulic Transmissivity of a Geo-synthetic Using a Constant Head

- American Society For Testing And Materials (ASTM) E84 Standard Test Method for Surface Burning Characteristics of Building Materials

- American Society For Testing And Materials (ASTM) E90 Standard Test Method for Laboratory Measurement of Airborne Sound Transmission Loss of Building Partitions

- American Society For Testing And Materials (ASTM) E96 Standard Test Methods for Water Vapor Transmission of Materials

- American Society For Testing And Materials (ASTM) E413 Standard Classification for Rating Sound Insulation

- American Society For Testing And Materials (ASTM) E492 Standard Test Method for Laboratory Measurement of Impact Sound Transmission Through Floor-Ceiling Assemblies Using the Tapping Machine

- American Society For Testing And Materials (ASTM) E989 Standard Classification for Determination of Impact Insulation Class (IIC)

- American Society For Testing And Materials (ASTM) E1155 Standard Test Method for Determining FF Floor Flatness and FL Floor Levelness

- American Society For Testing And Materials (ASTM) F710 Standard Practice for Preparing Concrete Floors to Receive Resilient Flooring

- American Society For Testing And Materials (ASTM) F1869 Standard Test Method for Measuring Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride

- American Society For Testing And Materials (ASTM) F2170 Standard Test Method for Determining Relative Humidity in Concrete Floor Slabs Using in-situ Probes

- American Society of Mechanical Engineers (ASME) - ASME A112.6.3 Floor and Trench Drains

- Canadian Sheet Steel Building Institute (CSSBI) Lightweight Steel Framing Binder {Publication 52M}

- Federal Housing Administration (FHA) Bulletin No. 750 Impact Noise Control in Multifamily Dwellings

- Housing and Urban Development (HUD) TS 28 A Guide to Airborne, Impact and Structure-borne Noise-Control in Multifamily Dwellings

- International Organization for Standardization (ISO) 13007 Standards for Grouts and Adhesives

- Materials And Methods Standards Association (MMSA) Bulletins 1-16

- Metal Lath/Steel Framing Association (ML/SFA) 540 Lightweight Steel Framing Systems Manual

- Steel Stud Manufacturers Association (SSMA) Product Technical Information and ICBO Evaluation Service, Inc. Report ER-4943P

- Terrazzo, Tile And Marble Association Of Canada (TTMAC) Specification Guide 09300 Tile Installation Manual

- Tile Council Of North America (TCNA) Handbook For Ceramic, Glass, and Stone Tile Installation

NOTE TO SPECIFIER: edit for applicable reference standards

1.10	SYSTEM DESCRIPTION

- Ceramic mosaic floor tile installed over concrete floor slabs using latex-modified portland cement mortar and latex portland cement grout joints.

- Quarry tile and base installed using latex modified portland cement mortar over a plastic portland cement mortar bed or over a cured (pre-floated) portland cement mortar bed with epoxy grouted joints.

NOTE TO SPECIFIER: The above systems are example descriptions; edit for additional applicable systems

  - SUBMITTALS

NOTE TO SPECIFIER: Edit for applicable requirements

- Submittal Requirements: Submit the following “Required LEED Criteria” certification items as listed below.  Refer to Division 1 for additional requirements:

  - A completed LEED Environmental Building Materials Certification Form.  Information to be

supplied generally includes:

    - Manufacturing plant locations for tile installation products.

    - LEED Credits as listed in Part 1.4B “LEED Credit Submittals”

    - Recycled content; pre-consumer or post-consumer; or;

Project specific information gathered using the LATICRETE LEED Project Certification Assistant available at https://laticrete.com/en/innovation-and-impact/green-leed/leed-project-certification-assistant.

  - UL GREENGUARD Certification Program For Chemical Emissions For Building Materials, Finishes

And Furnishings, UL 2818 or UL GREENGUARD Gold certificates provided by the tile installation materials manufacturer on UL GREENGUARD letterhead stating “This product has been UL GREENGUARD Gold Product Certified For Low Chemical Emissions by the UL Environment under the UL GREENGUARD Certification Program For Chemical Emissions For Building Materials, Finishes And Furnishings” for each tile installation product used to verify Low VOC product information.

  - Contractor’s certification of LEED Compliance: Submit Contractor’s certification verifying the

installation of specified LEED Compliant products.

  - Product Cut Sheets for all materials that meet the LEED performance criteria.  Submit Product Cut

Sheets with Contractor or Sub-contractor’s stamp, as confirmation that submitted products were

installed on Project.

  - Safety Data Sheets for all applicable products.

- LEED Credit Submittals for the following;

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit Building

Product Disclosure and Optimization – Environmental Product Declarations: Manufacturer’s Product

Specific (Type III) Environmental Product Declarations for LATICRETE Cement Mortar for Tile

Installation, LATICRETE Cement Grout for Tile Installation, and/or LATICRETE Cement Self-Leveling

Underlayment.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit Building

Product Disclosure and Optimization – Material Ingredients: Manufacturer’s product data for tile

installation materials, including Health Product Declaration (HPD) on HPD Collaborative letterhead.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit Building

Product Disclosure and Optimization – Sourcing of Raw Materials Option 2 (Recycled Content):

Manufacturer’s product data for tile installation materials.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 MR Credit:

Building Product Disclosure and Optimization – Sourcing of Raw Materials Option 2 (Regional

Materials): Product data indicating location of material manufacturer for regionally manufactured

Materials (within 100 miles of project site).

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 Edition MR Credit Construction and Demolition Waste Management: Path 1 (Divert 50% and Three Material Streams) Manufacturer’s packaging showing recycle symbol for appropriate disposition in construction waste management.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 Edition MR Credit Construction and Demolition Waste Management: Path 1 (Divert 75% and Four Material Streams) Manufacturer’s packaging showing recycle symbol for appropriate disposition in construction waste management.

  - LEED Reference Guide for Green Building Design and Construction, LEED v4 EQ Credit

Low-Emitting Materials: Manufacturer’s product data for tile installation materials, including UL

GREENGUARD Gold Certificate on UL GREENGUARD letterhead stating product VOC emissions.

8.   LEED Schools Reference Guide (Educational Projects Only), 2007 Edition Credit EQ 9 (Enhanced

Acoustical Performance): Impact noise reduction test reports and product data on sound control

product(s).

9.   LEED Schools Reference Guide (Educational Projects Only), 2007 Edition Credit EQ 10 (Mold

Prevention): Manufacturer’s packaging and/or data showing anti-microbial protection in product(s).

- Submit shop drawings and manufacturers' product data under provisions of Section (01 30 00)

(01 34 00)

- Submit samples of each type/style/finish/size/color of ceramic tile, mosaic, paver, trim unit or threshold under provisions of Section (01 30 00)  (01 34 00)

- Submit manufacturers' installation instructions under provisions of Section (01 30 00)  (01 34 00)

- Submit manufacturer's certification under provisions of Section (01405) that the materials supplied conform to ANSI A137.1 for ceramic tile or ANSI A137.2 for glass tile.

- Submit proof of warranty.

- Submit Health Product Declarations (HPD) for each tile installation material.

I.    Submit Product Specific (Type III) for Environmental Product Declarations for Cement Mortars for Tile

Installation, Cement Grouts for Tile Installation, and/or Cement Self-Leveling Underlayments specified.

- Submit sample of installation system demonstrating compatibility/functional relationships between adhesives, mortars, grouts and other components under provision of Section (01 30 00) (01 34 00).  Submit proof from tile or stone manufacturer or supplier verifying suitability of tile or stone for specific application and use; including dimensional stability, water absorption, freeze/thaw resistance (if applicable), resistance to thermal cycling, and other characteristics that the may project may require. These characteristics must be reviewed and approved by the project design professional(s).

- Submit list from manufacturer of installation system/adhesive/mortar/grout identifying a minimum of three (3) similar projects, each with a minimum of three (3) years service.

- For alternate materials, at least thirty (30) days before bid date submit independent laboratory test results confirming compliance with specifications listed in Part 2 - Products.

1.12	QUALITY ASSURANCE

NOTE TO SPECIFIER: Edit for applicable requirements

It is strongly recommended to use installers who have demonstrated a commitment to their craft and taken the time to stay current with the latest materials and methods. Requiring references and a portfolio along with a bid or estimate is a good way to ensure the installer has successfully completed work of similar size, scope, and complexity. Pools, exterior facades, mortar beds, shower pans, steam showers, etc. require different skills. Matching installer ability to the project at hand requires close evaluation of their experience, training, state licensing (where applicable), and certifications/credentials (where applicable). The Ceramic Tile Education Foundation (CTEF) provides a Contractor Questionnaire that can be used to aid in evaluating and comparing contractors (www.tilecareer.com).

Various programs administered by associations, non-profit educational organizations, unions, and private companies serve the tile industry by providing education, hands-on training, and evaluation of the skills and competency of installers and contractors. It is important to distinguish between the many programs available:

- Hands-on training

- Evaluation/certification of installation skills

- On-line training

- On-line knowledge evaluation (without a hands-on component)

As with all programs, the rigor and credibility of the program must also be considered.

The following non-profit programs are well-established and recognized by the Tile Council of North America’s (TCNA) Handbook Committee (listed alphabetically):

Ceramic Tile Education Foundation (CTEF) Certified Tile Installer Program: CTEF tests hands-on installation skills and knowledge. Installers must achieve the minimum required score on both tests to earn the “CTEF Certified Installer” designation. Contractors that employ CTEF Certified Installers are listed in the CTEF Contractor Directory, in the TCNA Handbook for Ceramic, Glass and Stone Tile and on the CTEF website. See www.tilecareer.org for more information.

International Masonry Institute (IMI) Contractor College Program: IMI conducts professional and technical courses for union masonry and tile contractors, which lead to certification in installation and project supervision. See www.imiweb.org for more information.

Journeyman Tile Layer Apprenticeship Programs: Installers recognized by the U.S. Department of Labor (DOL) as Journeyman Tile Layers are required to fulfill and document several years of training and on-the-job experience as apprentices to become Journeymen. The majority of these setters earn their Journeyman status through union-affiliated training programs, although some non-union tile contractors administer their own DOL-recognized apprenticeship programs and employ journeyman tile layers. Contractors that employ union Journeyman Tile Setters can be found through the union locals that list their signatory contractors, primarily the Bricklayer and Allied Craftworkers (BAC) and the United Brotherhood of Carpenters (UBC). See www.bacweb.org and www.carpenters.org for more information.

National Tile Contractors Association (NTCA) Five Star Contractor Program: NTCA is a tile contractors association, with membership open to all tile contractors. Their Five Star program is a peer review program to recognize NTCA members who have demonstrated a track record of providing successful installations. Earning the Five Star designation requires recommendations from customers, suppliers, and peers as well as participation in continuing education, training, and safety programs. See www.tile-assn.com for more information.

Tile Contractors’ Association of America (TCAA) Trowel of Excellence Program: TCAA is a contractors association for BAC signatory contractors. Its Trowel of Excellence program is a peer review program to recognize TCAA members who have demonstrated a track record of providing successful installations. Earning the Trowel of Excellence designation requires letters of reference, submittal of a detailed project description and photos, employee participation in educational programming, and proof of financial responsibility. See www.tcaainc.org for more information.

- Tile Manufacturer (single source responsibility): Company specializing in ceramic tile, mosaics, pavers, trim units and/or thresholds with three (3) years minimum experience.  Obtain tile from a single source with resources to provide products of consistent quality in appearance and physical properties.

- Installation System Manufacturer (single source responsibility): Company specializing in adhesives, mortars, grouts and other installation materials with ten (10) years minimum experience and ISO 9001-2008 certification.  Obtain installation materials from single source manufacturer to insure consistent quality and full compatibility.

- Submit laboratory confirmation of adhesives, mortars, grouts and other installation materials:

  - Identify proper usage of specified materials using positive analytical method.

  - Identify compatibility of specified materials using positive analytical method.

  - Identify proper color matching of specified materials using a positive analytical method.

- Installer qualifications: company specializing in installation of ceramic tile, mosaics, pavers, trim units and thresholds with five (5) years documented experience with installations of similar scope, materials and design.

1.13	MOCK-UPS

- Provide mock-up of each type/style/finish/size/color of ceramic tile, mosaics, pavers, trim unit and threshold, along with respective installation adhesives, mortars, grouts and other installation materials, under provisions of Section (01400) (01405).

1.14	PRE-INSTALLATION CONFERENCE

Pre-installation conference: At least three weeks prior to commencing the work attend a meeting at the jobsite to discuss conformance with requirements of specification and job site conditions.  Representatives of owner, architect, general contractor, tile subcontractor, Tile Manufacturer, Installation System Manufacturer and any other parties who are involved in the scope of this installation must attend the meeting.

1.15	DELIVERY, STORAGE AND HANDLING

- Acceptance at Site: deliver and store packaged materials in original containers with seals unbroken and labels, including grade seal, intact until time of use, in accordance with manufacturer's instructions.

- Store ceramic tile and installation system materials in a dry location; handle in a manner to prevent chipping, breakage, and contamination.

- Protect latex additives, organic adhesives, epoxy adhesives and sealants from freezing or overheating in accordance with manufacturer's instructions; store at room temperature when possible.

- Store portland cement mortars and grouts in a dry location.

1.16	PROJECT/SITE CONDITIONS

- Provide ventilation and protection of environment as recommended by manufacturer.

- Prevent carbon dioxide damage to ceramic tile, mosaics, pavers, trim, thresholds, as well as adhesives, mortars, grouts and other installation materials, by venting temporary heaters to the exterior.

C.   Maintain ambient temperatures not less than 50ºF (10ºC) or more than 100ºF (38ºC) during installation and for a minimum of seven (7) days after completion.  Setting of portland cement is retarded by low

temperatures.  Protect work for extended period of time and from damage by other trades.  Installation with latex portland cement mortars requires substrate, ambient and material temperatures at least 37ºF (3ºC).  There should be no ice in slab.  Freezing after installation will not damage latex portland cement mortars. Protect portland cement based mortars and grouts from direct sunlight, radiant heat, forced ventilation (heat & cold) and drafts until cured to prevent premature evaporation of moisture. Epoxy mortars and grouts require surface temperatures between 60ºF (16ºC) and 90ºF (32ºC) at time of installation. It is the General Contractor’s responsibility to maintain temperature control.

1.17	SEQUENCING AND SCHEDULING

- Coordinate installation of tile work with related work.

- Proceed with tile work only after curbs, vents, drains, piping, and other projections through substrate have been installed and when substrate construction and framing of openings have been completed.

NOTES FOR SPECIFIER:  Edit for project specific sequence and scheduling

1.18      WARRANTY

The manufacturer of adhesives, mortars, grouts and other installation materials shall provide a written twenty five (25) year warranty, which covers materials and labor - reference LATICRETE Warranty Data Sheet 025.0 for complete details and requirements.  For exterior facades over steel or wood framing, the manufacturer of adhesives, mortars, grouts and other installation materials shall provide a written fifteen (15) year warranty, which covers replacement of LATICRETE products only – reference LATICRETE Warranty Data Sheet 230.15 for complete details and requirements.

1.19	MAINTENANCE

Submit maintenance data under provisions of Section 01 73 00. Include cleaning methods, cleaning solutions recommended, stain removal methods, as well as polishes and waxes recommended.

1.20	EXTRA MATERIALS STOCK

Upon completion of the work of this Section, deliver to the Owner 2% minimum additional tile and trim shape of each type, color, pattern and size used in the Work, as well as extra stock of adhesives, mortars, grouts and other installation materials for the Owner's use in replacement and maintenance. Extra stock is to be from same production run or batch as original tile and installation materials.

PART 2 - PRODUCTS

2.1	TILE MANUFACTURERS

Subject to compliance with paragraphs 1.12 and performance requirements, provide products by one of the following manufacturers:

NOTE TO SPECIFIER: Provide list of acceptable tile manufacturers.

2.2	WALL TILE MATERIALS

NOTE TO SPECIFIER: edit for each tile type

- Ceramic Tile:

- Grade:

- Size:

- Edge:

- Finish:

- Color:

- Special shapes:

- Location:

2.3	FLOOR TILE MATERIALS

NOTE TO SPECIFIER: edit for each tile type

- Ceramic Tile:

- Grade:

- Size:

- Edge:

- Finish:

- Color:

- Special shapes:

- Location:

2.4	CERAMIC TILE INSTALLATION MATERIALS MANUFACTURER

- LATICRETE International, Inc., 1 Laticrete Park North, Bethany, CT 06524-3423 USA Phone 800-243-4788, (203) 393-0010 technicalservices@laticrete.com;  https://laticrete.com;  https://laticrete.com/en/innovation-and-impact/green-leed

NOTE TO SPECIFIER: Use either the following performance specification or the proprietary specification.

2.5	PERFORMANCE SPECIFICATION - TILE INSTALLATION ACCESSORIES

- Waterproofing Membrane to be thin, cold applied, single component liquid and load bearing. Reinforcing fabric to be non-woven rot-proof specifically intended for waterproofing membrane.  Waterproofing Membrane to be non-toxic, non-flammable and non-hazardous during storage, mixing, application and when cured. It shall be certified by IAPMO and ICC approved as a shower pan liner and shall also meet the following physical requirements:

  - Hydrostatic Test (ASTM D4068):              	     Pass

  - Elongation @ break (ASTM D751):	20-30%

  - System Crack Resistance (ANSI A118.12):	Pass (High)

  - 7 day Tensile Strength (ANSI A118.10):                      >265 psi (1.8 MPa)

  - 7 day Shear Bond Strength (ANSI A118.10)               >200 psi (1.4 MPa)

  - 28 Day Shear Bond Strength (ANSI A118.4):	>214 psi (1.48 – 2.4 MPa)

  - Service Rating (TCA/ASTM C627): 	Extra Heavy

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

B.    Epoxy Waterproofing Membrane to be 3 component epoxy, trowel applied specifically designed to be used under ceramic tile, stone, masonry veneer, or brick and requires only 24 hours prior to flood testing:

  - Breaking Strength (ANSI A118.10):              	     450-530 psi (3.1-3.6 MPa)

  - Waterproofness (ANSI A118.10):	No Water penetration

  - 7 day Shear Bond Strength (ANSI A118.10):              110-150 psi (0.8-1 MPa)

  - 28 Day Shear Bond Strength (ANSI A118.10):	90-120 psi (0.6–0.83 MPa)

  - 12 Week Shear Bond Strength (ANSI A118.10):        110-130 psi (0.8-0.9 MPa)

  - Total VOC Content:                                                     <3.4 g/L

C.   Crack Suppression Membrane to be thin, cold applied, single component liquid and load bearing.  Reinforcing fabric (if required or used) to be non-woven, rot-proof specifically intended for crack suppression membrane.  Materials to be non-toxic, non-flammable, and non-hazardous during storage, mixing, application and when cured. Crack Suppression Membrane shall also meet the following physical requirements:

  - Elongation @ break (ASTM D751):	20-30%

  - System Crack Resistance (ANSI A118.12)	Pass (High)

  - 7 day Tensile Strength (ANSI A118.10):                      265 – 300 psi (1.8 – 2.0 MPa)

  - 7 day Shear Bond Strength (ANSI A118.10):              200 – 275 psi (1.4 – 1.9 MPa)

  - 28 Day Shear Bond Strength (ANSI A118.4):	>214 – 343 psi (1.48 – 2.4 MPa)

  - Service Rating (TCA/ASTM C627): 	Extra Heavy

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

D.  Wire Reinforcing:  2 inch x 2 inch (50 x 50 mm) x 16 ASW gauge or 0.0625 inch (1.6mm) diameter

galvanized steel welded wire mesh complying with ANSI A108.02 3.7, ASTM A185 and ASTM A82.

E.  Cleavage membrane: 15 pound asphalt saturated, non-perforated roofing felt complying with ASTM  D226, 15 pound coal tar saturated, non-perforated roofing felt complying with ASTM D227 or 4.0 mils (0.1 mm) thick polyethylene plastic film complying with ASTM D4397.

F.   Cementitious backer board units: size and thickness as specified, complying with ANSI A118.9.

G.   Thresholds:  Provide marble saddles complying with ASTM C241 for abrasion resistance and ASTM

C503 for exterior use, in color, size, shape and thickness as indicated on drawings.

NOTE TO SPECIFIER:  Edit applicable tile installation accessories.

PERFORMANCE SPECIFICATION - TILE INSTALLATION MATERIALS

- Tile Board shall be high density, waterproof extruded polystyrene core with a reinforced, waterproof membrane on both sides.  Board to be available in multiple thicknesses and suitable for use on interior walls, floors, ceilings, shower/tub surrounds, and steam rooms, as well as meet the following physical requirements:

  - Water Vapor Transmission (ASTM E96 Method E):   0.034 Perms

  - Compressive Strength (ASTM D1621):                       >55 psi (0.38 MPa)

  - Flexural Strength (IAPMO Z124):	Pass

4.    Linear Expansion (ASTM D1037):	-0.04%

- Sound Abatement & Crack Isolation Mat shall be load bearing, shock and vibration resistant.  It shall be certified by independent laboratory testing to meet the specified acoustical performance when installed in a Floor Assembly with a 6" (150mm) concrete slab, as well as meet the following physical requirements:

  - Service Rating (ASTM C627):                                     Moderate

  - Installed Weight (ASTM C905 Modified):	4.3 lbs./ft2 (21.1 kg/m2)

  - Delta Impact Insulation Class (ΔIIC; ASTM E2179):	22

- Sound Abatement & Crack Suppression Adhesive shall comply with ANSI A118.12, provide an Extra Heavy rating, UL GREENGUARD Gold compliant, and provide a minimum ΔIIC of 15:

1.   Service Rating (ASTM C627):                   	Extra Heavy

2.   Delta Impact Insulation Class (ΔIIC; ASTM E2179):    15

3.   Point Load (ANSI A118.12 5.2):                                   >1,000 psi (6.9 MPa)

4.   Minimum Shear Bond Strength (ANSI A118.12):         100psi (0.7 MPa)

- Uncoupling Membrane shall comply with ANSI A118.12, provide an Extra Heavy rating and allow for use with ANSI A118.4 thin-bed mortars:

1.   Service Rating (ASTM C627):	Extra Heavy

2.   System Crack Resistance (ANSI A118.12 5.4):	Pass (High)

3.   Point Load (ANSI A118.12 5.2):	Pass

- Moisture Vapor Reduction to be epoxy based and UL GREENGUARD Gold compliant as well as meet the following physical requirements:

1.    Shear Bond to Concrete (ANSI A118.12-5.1.5):          >285 psi (2.0 MPa)

2.    Alkalinity Resistance (ASTM C267):                            Pass

3.    Permeability (ASTM F1869):                                        9.7 lbs/1,000ft2/24 hours down to 0.2

lbs/1,000 ft2/24hours (248 µg/s•m2 down to

11 µg/s•m2)

4.   Total VOC Emissions:	 ≤0.22 mg/m3

- Latex Portland Cement Mortar for thick beds, screeds, leveling beds and scratch/plaster coats to be weather, frost, shock resistant, UL GREENGUARD Gold compliant, and meet the following physical requirements:

  - Compressive Strength (ANSI A118.4 Modified):         >4,000 psi (27.6 MPa)

  - Water Absorption (ANSI A118.6):	≤ 5%

  - Service Rating (TCA/ASTM C627):                             Extra Heavy

  - Smoke & Flame Contribution (ASTM E84 Modified):  0

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Self-Leveling Underlayment shall be mixed with water to produce a pumpable, fast setting, free flowing cementitious underlayment which can be poured from 1/8” to 1 ¼” (3 - 32mm) thick in one pour.

  - Flexural Strength (ASTM C1708):	            >840 psi (5.8 MPa)

  - 28 Day Compressive Strength (ANSI A118.4 Mod.):  >4,000 psi (27.6 MPa)

  - Tensile Strength (ANSI A118.7):                                 >270 psi (1.9 MPa)

  - Time To Foot Traffic @ 70˚F (21˚C):                          1 – 4 Hours

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Epoxy Adhesive to be chemical resistant 100% solids epoxy with high temperature resistance, UL GREENGUARD Gold compliant, conform to ISO R2, and meet the following minimum physical requirements:

  - Compressive strength (ANSI A118.3):	>5,000 psi (34.4 MPa)

  - Shear Bond Strength (ANSI A118.3):	>1,250 psi (8.6 MPa)

  - Thermal Shock Resistance (ANSI A118.3):                >600 psi (4.1 MPa)

  - Tensile Strength (ANSI A118.3):                                 >1,400 psi (9.6 MPa)

  - Shrinkage (ANSI A118.3):                                           0 – 0.1%

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

  - Cured Epoxy Adhesive to be chemically and stain resistant to ketchup, mustard, tea, coffee, milk, soda, beer, wine, bleach (5% solution), ammonia, juices, vegetable oil, detergents, brine, sugar, cosmetics and blood, as well as chemically resistant to dilute food acids, dilute alkalis, gasoline, turpentine and mineral spirits.

- Latex Portland Cement Thin Bed Mortar for thin set and slurry bond coats to be weather, frost, shock resistant, non-flammable, UL GREENGUARD Gold compliant, conform to ISO C2TES1 and meet the following physical requirements:

  - Tensile adhesion strength (ISO 13007-2 4.4.2):	>260 psi (1.8 MPa)

  - 28 day shear bond strength (ANSI A118.15):	>475 psi (3.3 MPa)

  - 7 day water immersion shear (ANSI A118.15):	>250 psi (1.7 MPa)

  - Smoke & Flame Contribution (ASTM E84 Modified):  0

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Latex Portland Cement Large, Heavy Tile Mortar for thin set and slurry bond coats to be weather, frost, shock resistant, non-flammable, UL GREENGUARD Gold compliant, and meet the following physical requirements:

  - 28 Day shear bond strength (ANSI A118.15):	≥500 psi (3.45 MPa)

  - 28 Day Freeze/Thaw Cycling (ANSI A118.15):	≥400 psi (2.76 MPa)

  - 7 day water immersion shear (ANSI A118.15):           ≥350 psi (2.4 MPa)

  - Sag Resistance (ANSI A118.15):                                0 mm

  - Total VOC Emissions:                                                 ≤0.22 mg/m3

- Organic Adhesive shall be a non-flammable, water resistant, latex adhesive and shall meet the following physical requirements:

  - Open Time (ANSI A136.1):	70 minutes @ 75°F (24°C)

  - Color:	White

  - Density (ANSI A136.1):	13.2 lbs/gal (1.6 kg/l)

  - Total VOC Content	<36.00 g/L

- Epoxy Grout (Industrial) to be non-flammable, chemical resistant 100% solids epoxy with high temperature resistance, UL GREENGUARD Gold compliant,  and meeting the following physical requirements:

  - Initial Set Time (ANSI A118.5):	Pass (4 hours)

  - Service Set Time (ANSI A118.5):	Pass (< 7 days)

  - Shrinkage (ANSI A118.3):	0.07%

  - Sag (ANSI A118.3):	Pass (No sag)

  - Shear Bond Strength (ANSI A118.3; quarry tile):	2,200 psi (15.2 MPa)

  - Compressive Strength (ANSI A118.3):	8,300 psi (57.2 MPa)

  - Tensile Strength (ANSI A118.5):	3,000 psi (20.7 MPa)

  - Thermal Shock Resistance (ANSI A118.3):	2,100 psi (14.5 MPa)

  - Total VOC Emissions:	≤0.22 mg/m3

  - Cured Epoxy Grout to be chemically and stain resistant to ketchup, mustard, tea, coffee, milk, soda, beer, wine, bleach (3% solution), ammonia, juices, vegetable oil, detergents, brine, sugar, cosmetics, and blood, as well as being chemically resistant to dilute food/mineral acids, gasoline and mineral spirits.

- Epoxy Grout (Commercial/Residential) shall be non-toxic, non-flammable, non-hazardous during storage, mixing, application and  when cured, UL GREENGUARD Gold compliant,  and shall meet the following physical requirements:

  - Compressive Strength (ANSI A118.3):                                3,800 psi (26.2 MPa)

  - Shear Bond Strength (ANSI A118.3):                                  1,100 psi (7.6 MPa)

  - Tensile Strength (ANSI A118.3):                                         1,100 psi (7.6 MPa)

  - Thermal Shock (ANSI A118.3):                                            >800 psi (5.5 MPa)

  - Water Absorption (ANSI A118.3):                                        <0.05%

  - Vertical Joint Sag (ANSI A118.3):                                        Pass

  - Total VOC Emissions:                                                          ≤0.22 mg/m3

  - Cured Epoxy Grout to be chemically and stain resistant to ketchup, mustard, tea, coffee, milk, soda, beer, wine, bleach (5% solution), ammonia, juices, vegetable oil, brine, sugar, cosmetics, and blood, as well as chemically resistant to dilute acids and dilute alkalis.

- Latex Portland Cement Grout to be weather, frost and shock resistant, UL GREENGUARD Gold compliant, as well as meet the following physical requirements:

  - Compressive Strength (ANSI A118.7):	 4,500 psi (31 MPa)

  - Tensile Strength (ANSI A118.7):                                  500 psi (3.4 MPa)

  - Flexural Strength (ANSI A118.7):                                 1,250 psi (8.6 MPa)

  - Water Absorption (ANSI A118.7):	 < 5%

  - Linear Shrinkage (ANSI A118.7):                                 < 0.05 %

  - Smoke & Flame Contribution (ASTM E84 Modified):   0

  - Total VOC Emissions:                                                  ≤0.22 mg/m3

N.   Expansion and Control Joint Sealant to be a one component, neutral cure, exterior grade silicone sealant and meet the following requirements:

  - Tensile Strength (ASTM C794):	280 psi (1.9 MPa)

  - Hardness (ASTM D751; Shore A):                              25 (colored sealant) /15 (clear sealant)

  - Weather Resistance (QUV Weather-ometer):            10,000 hours (no change)

  - VOC Emissions:	≤0.5 mg/m3

  - VOC Content:	≤37.16 g/L

O.   Roof Decks (and other exterior paving applications over occupied/storage spaces) shall consist of a Primary Roofing/Waterproofing Membrane, as specified in Section 0700 (q.v.), and a lightweight, frost/weather resistant installation system for tile, pavers, brick and stone that provides integral subsurface drainage and meets the following physical requirements:

  - Compressive Strength (ASTM C109 Modified):	3,000 psi (20.7 MPa)

  - Hydraulic Transmissivity (ASTM D4716):	1.6 gal./minute (6.1 L/minute)

  - Service Rating (ASTM C627):                                      Extra Heavy

P.   Spot Bonding Epoxy Adhesive for installing tile, brick, masonry veneer, and stone over vertical and overhead surfaces shall be high strength, high temperature resistant, non-sag and shall meet the following physical requirements:

  - Thermal Shock Resistance (ANSI A118.3):	>1,000 psi (6.9 MPa)

  - Water Absorption (ANSI A118.3):                                0.1 %

  - Compressive Strength (ANSI A118.3):	>8,300 psi (57.2 MPa)

  - Shear Bond Strength (ANSI A118.3 Modified):	>730 psi (5 MPa)

Q.   Sealer shall be water-based and provide maximum protection against both water- and oil- based stains, and meet the following requirements:

1.    Surface Traffic: 6 – 8 hours

2.    Full Cure in 24 – 72 hours

3.    VOC Compliant: 12 g/L (low solids coating)

4.    Natural Look Sealer

NOTE TO SPECIFIER:  Edit applicable tile installation materials.

2.6	PROPRIETARY SPECIFICATION - TILE INSTALLATION ACCESSORIES

Installation accessories as manufactured by LATICRETE International, Inc., 1 LATICRETE Park North, Bethany, CT  06524-3423 USA. Phone 800-243-4788, www.laticrete.com

- Waterproofing Membrane: LATICRETE HYDRO BAN® ** as manufactured by LATICRETE International, Inc.

- Epoxy Waterproofing Membrane: LATAPOXY® Waterproof Flashing Mortar as manufactured by LATICRETE International, Inc.

- Crack Suppression Membrane: LATICRETE® HYDRO BAN® ** as manufactured by LATICRETE International, Inc.

NOTE TO SPECIFIER:  Edit applicable tile installation accessories.

PROPRIETARY SPECIFICATION - TILE INSTALLATION MATERIALS

Installation materials as manufactured by LATICRETE International, Inc., 1 LATICRETE Park North, Bethany, CT  06524-3423 USA. Phone 800-243-4788, www.laticrete.com; www.laticrete.com/green

- Tile Board: LATICRETE HYDRO BAN Board as manufactured for LATICRETE International, Inc.

- Sound Control Underlayment: LATICRETE 170.5 Sound & Crack Isolation Mat as manufactured for LATICRETE International, Inc.

- Sound & Crack Isolation Adhesive: LATICRETE 125 TRI MAX** as manufactured by

LATICRETE International, Inc.

C.   Uncoupling Membrane: LATICRETE STRATA_MAT™ as manufactured for LATICRETE International, Inc.

D.   Electric Radiant Floor Heat System: LATICRETE STRATA_HEATTM Mat with

LATICRETE STRATA_HEAT Spliceless Wire as manufactured for LATICRETE International, Inc.

- Moisture Vapor Reduction: LATICRETE VAPOR BAN™ E as manufactured by LATICRETE International, Inc.

- Latex-Portland Cement Mortar for thick beds, screeds, leveling beds and scratch/plaster coats: LATICRETE 3701 Fortified Mortar Bed** as manufactured by LATICRETE International, Inc.

- Self-Leveling Underlayment: LATICRETE NXT LEVEL PLUS™ as manufactured by LATICRETE International, Inc.

- Epoxy Adhesive: LATAPOXY 300 Adhesive** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Thin Bed Mortar: LATICRETE 254 PLATINUM™** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Thin Bed Mortar: LATICRETE 254 PLATINUM PLUS** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Thin Bed Mortar: LATICRETE 253 Gold** as manufactured by LATICRETE International, Inc.

- Medium Bed Mortar: LATICRETE MULTIMAX™ LITE** as manufactured by LATICRETE International, Inc.

- Organic Adhesive: LATICRETE 15 Premium Mastic as manufactured for LATICRETE International, Inc.

- Epoxy Grout (Industrial): LATICRETE SPECTRALOCK® 2000 IG** as manufactured by LATICRETE International, Inc.

- Epoxy Grout (Commercial/Residential): LATICRETE SPECTRALOCK® PRO Premium Grout** as manufactured by LATICRETE International, Inc.

- Latex Portland Cement Grout: LATICRETE PERMACOLOR® Select** as manufactured by LATICRETE International, Inc.

- Expansion and Control Joint Sealant: LATICRETE LATASIL™ ^ as manufactured for LATICRETE International, Inc.

- Roof Deck: LATICRETE Plaza & Deck System as manufactured by LATICRETE International, Inc.

- Spot Bonding Epoxy Adhesive: LATAPOXY 310 Stone Adhesive as manufactured for LATICRETE International, Inc.

- Sealer: STONETECH BulletProof® Sealer as manufactured for LATICRETE International, Inc.

**   UL GREENGUARD Certified For Low Chemical Emissions (ULCOM/GG 2818) and UL GREENGUARD Gold Certified For Low Chemical Emissions (ULCOM/GG UL 2818)

^     Independently tested per CDPH v1.2 for Low VOC Emissions to meet ≤0.5mg /m3.

END OF SECTION

©2024 LATICRETE International, Inc., all rights reserved

PART 3 - EXECUTION

3.1	SUBSTRATE EXAMINATION

A.   Verify that surfaces to be covered with ceramic tile, porcelain tile, mosaics, stone, trim or waterproofing are:

  - Sound, rigid and conform to good design/engineering practices;

  - Systems, including the framing system and panels, over which tile or stone will be installed shall be in conformance with the International Residential Code (IRC) for residential applications, the International Building Code (IBC) for commercial applications, or applicable building codes.  The project design should include the intended use and necessary allowances for the expected live load, concentrated load, impact load, and dead load including the weight of the finish and installation materials. In addition to deflection considerations, above ground installations are inherently more susceptible to vibration. When concentrated loads (scissor lifts, pallet jacks, automobiles, forklifts, etc…) will be used on an above ground tiled, floor the project design professionals shall specify a substrate to accommodate the concentrated loads. Consult grout, mortar, and membrane manufacturer to determine appropriate installation materials for above ground installations. A crack isolation membrane and higher quality setting materials can increase the performance capabilities of above ground applications. However, the upgraded materials cannot mitigate structural deficiencies including floors not meeting code requirements and/or over loading or other abuse of the installation in excess of design parameters. Maximum allowable floor member live load and concentrated load deflection shall not exceed L/360 for tile or L/480 for stone, where L is the clear span length of the supporting member per applicable building code;

  - The actual weight of materials and construction assemblies, including concentrated dead loads of fixed service and other equipment, shall be utilized as prescribed by state and local building codes to estimate dead loads for the purpose of structural design;

  - For thin-bed ceramic tile installations when a cementitious bonding material will be used, including medium bed mortar: maximum allowable variation in the tile substrate – for tiles with edges shorter than 15” (375mm), maximum allowable variation is ¼” in 10’ (6mm in 3m) from the required plane, with no more than 1/16” variation in 12” (1.5mm variation in 300mm) when measured from the high points in the surface. For tiles with at least one edge 15” (375mm) in length, maximum allowable variation is 1/8” in 10’ (3mm in 3m) from the required plane, with no more than 1/16” variation in 24” (1.5mm variation in 600mm) when measured from the high points in the surface. For modular substrate units, such as exterior glue plywood panels or adjacent concrete masonry units, adjacent edges cannot exceed 1/32” (0.8mm) difference in height. Should the architect/designer require a more stringent finish tolerance (e.g. 1/8” in 10’ [3mm in 3m]), the subsurface specification must reflect that tolerance, or the tile specification must include a specific and separate requirement to bring the subsurface tolerance into compliance with the desired tolerance. For thick bed (mortar bed) ceramic and stone tile installations and self-leveling methods: maximum allowable variation in the installation substrate to be ¼” in 10’ (6mm in 3m);

  - Lateral and other bracing must be constructed as prescribed by code and/or engineered wood manufacturers’ literature to achieve specified design deflection values;

  - Clean and free from dust, dirt, oil, grease, sealers, curing compounds, laitance, efflorescence, form oil, loose plaster, paint, and scale per ANSI A108.02 4.1.1;

  - To fully evacuate water, shower pan membranes and bonded waterproofing membranes in wet areas must slope to and connect with a drain. Plumbing code typically requires membranes to be sloped a minimum of ¼” per ft. (6mm per 300mm) and extend at least 3” (75mm) above the height of the curb or threshold. Account for the perimeter floor height required to form adequate slopes. Membranes must be installed over the other horizontal surfaces in wet areas subject to deterioration, like shower seats. They must be sloped and configured to direct water to the membrane connected to the drain. The weep holes of clamping ring drains enable water to pass from the membrane into the plumbing system. Crushed stone or tile, or other positive weep protectors, placed around/over weep holes help prevent their blockage. To form a watertight seal, membranes must have adequate contact with the clamping ring of the drain

  - Not leveled with gypsum or asphalt based compounds; For substrates scheduled to receive a waterproofing and/or crack isolation membrane, maximum amount of moisture in the concrete/mortar bed substrate should not exceed 5 lbs./1,000 ft2 / 24 hours (283 µg/s•m2) per ASTM F1869 or 75% relative humidity as measured with moisture probes per ASTM F2170. Consult with finish materials manufacturer to determine the maximum allowable moisture content for substrates under their finished material.

  - Steam rooms are highly specialized applications. Design and installation are critical to avoid damage to adjoining materials from vapor migration.  Design criteria must include consideration of necessary insulation and temperature/humidity differential.

10.  Dry as per American Society for Testing and Materials (ASTM) D4263 “Standard Test for Determining Moisture in Concrete by the Plastic Sheet Method.”

NOTE: Steam unit design must take into consideration the effect of moisture vapor transmission (MVT) on opposite side of steam unit walls. MVT can cause efflorescence and can affect paints, coatings and adhered finishes.

- Concrete surfaces shall also be:

  - Cured a minimum of 28 days @ 70˚F (21˚C), including an initial seven (7) day period

of wet curing;

NOTE TO SPECIFIER: LATICRETE® Latex Portland Cement Mortars do not require a minimum cure time for concrete substrates or mortar beds;

  - Wood float finished, or better, if the installation is to be done by the thin bed method;

- Advise General Contractor and Architect of any surface or substrate conditions requiring correction before tile work commences.  Beginning of work constitutes acceptance of substrate or surface conditions.

- Environmental Classification (TCNA): Res 4; Com 4. Consult Tile Council of North America Handbook for Ceramic, Glass, and Stone Tile Installation for more information.

3.2	SURFACE PREPARATION

A.   REQUIREMENTS

Steam Rooms require a primary shower pan liner and waterproofing membrane on all surfaces to prevent moisture from penetrating adjoining spaces. Additionally, a vapor diffusion retarder (6 mil thick polyethylene sheeting or #15 Builders Felt) must be installed over the steel framing and behind the cement backer board. Vapor diffusion retarder shall be designed for relative temperature exposure. Install vapor diffusion retarder so that it laps over the shower pan waterproofing membrane so that condensation can drain into the shower pan (not behind it) - see associated detail SR-614B.  All steam rooms will require adequate insulation on walls and ceilings to reduce moisture condensation caused by temperature variations. Slope ceilings 2” per foot (50mm per 300mm) minimum to avoid condensation from dripping onto occupants. Install open slip joints in all corners between walls and ceiling, as well as to divide areas that exceed 16’ (480cm) in length.  Structure to receive the installation assembly must be sound, solid, well bonded, stripped clean and free from dust, wax, grease, sealer, and all other contamination that may reduce or prevent adhesion per ANSI A108.02 (4.0).

- Bonded Thick Bed - Pitch Layer Over Floor Substrate - To provide pitch over a concrete deck, prepare a LATICRETE Latex Leveling Bed mix (see §3.4C thick bed mortar material below applied over a slurry bond coat consisting of LATICRETE® 254 Platinum). Apply mortar over dampened substrate. Pitch layer ¼” per 1’ (6mm per 300mm) per ANSI A108.1A (2.3.4).

*  NOTE to Specifier: LATICRETE® 254 Platinum Plus can replace LATICRETE 254 Platinum as the slurry bond coat.

C. 	(List other Substrates as required and means of preparation as required)

(Insert any Special Means of Preparation – In addition to the surface preparation requirements listed above; …)

NOTE TO SPECIFIER: The above are example surface categories; edit for project specific surfaces and conditions.

D.   The minimum uniformly distributed live load and minimum concentrated live loads, wherever such loads shall occur, shall be provided for as prescribed by state and local building codes.

3.3	INSTALLATION - ACCESSORIES

(edit as required)

- Metal Edge Trim LATICRETE Profiles & Trims fulfill a wide range of needs including edge protection, floor transitions, decorative and more. Installed indoors and outdoors, they can be used with multiple floor coverings such as tile and stone, terrazzo, wood and LVT. Create unique designs with a selection of finishes and colors in kitchens and bathrooms, commercial and residential applications, and everything in between.

Application:

    - Select the correct size of profile according to the tile thickness.

    - Prior to installing the tile, make sure the profiles, corners, and connectors are accurately measured and dry-fitted. Measure and mark the profile to the correct length before cutting.

    - Apply tile adhesive with a margin or notched trowel to the area where the profile will be installed.

    - Firmly press the profile into the adhesive, allowing the adhesive to flow through octagonal cutouts in the mounting leg.

    - Adjust and straighten the profile if necessary. Using an appropriate notched trowel and adhesive for the tile to be installed, add more adhesive over the mounting leg and surface fully embedding the mounting leg of the profile.

    - Press the tile firmly into the adhesive to achieve full coverage, ensuring the profile and tile are aligned and flush. Leave a 1/16" to 1/8" gap between the profile and tile for grouting.

    - Continue tiling the rest of the area. Immediately after installing the profiles and tile, clean the surface of the profile to remove any residual adhesive or cement material with clean fresh water and a sponge or microfiber cloth.

NOTE: The use of stainless steel profiles in grade 316 for steam showers/steam rooms is preferred.

Use the following LATICRETE System Materials:

LATICRETE Profiles & Trims

References:

Floor Method: Floor Method

Method With Cove Base: Method With Cove Base

Wall or countertop method: Wall or countertop method

Ej-171 And All Floor and Wall Methods: Ej-171 And All Floor and Wall Methods

3.4        INSTALLATION – TILE, BRICK, MASONRY VENEER, & STONE

- General: Install in accordance with current versions of American National Standards

Institute, Inc. (ANSI) “A108 American National Standard Specifications for

Installation of Ceramic Tile” and Tile Council of North America “Handbook for Ceramic, Glass, and Stone Tile Installation”.  Cut and fit ceramic tile, porcelain tile, glass tile, or stone neatly around corners, fittings, and obstructions.  Perimeter pieces to be minimum half tile or stone. Chipped, cracked, split pieces and edges are not acceptable.  Make joints even, straight, plumb and of uniform width to tolerance +/- 1/16" over 8’ (1.5mm in 2.4m). Install divider strips at junction of flooring and dissimilar materials. When glass tile is used, consult glass tile manufacturer for membrane options and recommendations. Where installation will be subjected to freeze/thaw cycles, snow and ice accumulation, and/or snow melting salts/chemicals, degradation can occur over time.

- Wall Board (LATICRETE® HYDRO BAN® Board):

Fastening: Wood Studs: Nominal Dimensions – 2” x 4” (51 x 102mm) minimum with maximum span of 16” (406mm) o.c. use a minimum of 1/2” (12mm) LATICRETE HYDRO BAN® Board, and for 19.2” (488mm) o.c. stud spacing use a minimum of 5/8” (16mm) LATICRETE HYDRO BAN Board. Fasten boards directly to studs using the appropriate length LATICRETE HYDRO BAN Board Screw for the thickness of the LATICRETE HYDRO BAN Board. Screws should be spaced 12” o.c. (305 mm). All screw heads should be countersunk flush with surface of the board.

Fastening: Steel Studs: Minimum Thickness – 25 gauge with maximum span of 16” o.c. (406mm). Use a minimum of 1/2” (12mm) LATICRETE HYDRO BAN Board. Fasten boards directly to studs using the 1 5/8” (41mm) LATICRETE HYDRO BAN Board screw. Screws should be spaced 12” o.c. (305mm). All screws should be countersunk flush with surface of the board.

INSTALLATION:

The following steps must be followed to maintain the waterproof integrity of LATICRETE HYDRO BAN Board.  Install HYDRO BAN Board as outlined below but the 1 ¼” (32 mm) LATICRETE HYDRO BAN Tab Washers must be used with the 1 5/8” (42.5mm) or longer LATICRETE HYDRO BAN Board Screws.

1. Fasten LATICRETE® HYDRO BAN® Board to the ceiling studs by using LATICRETE HYDRO BAN Board Screws and LATICRETE HYDRO BAN Tab Washers following fastener spacing as outlined above (Fastening: Steel Studs).  Ensure that the ceiling framing is sloped at 2” per foot (50 mm per 300 mm) minimum.

2. Beginning at the bottom of the wall, install LATICRETE HYDRO BAN Board to the wall studs by using the LATICRETE HYDRO BAN Board Screws following the spacing outlined in the fastening section above. For installations with LATICRETE HYDRO BAN Pre-Sloped Shower Pans first apply a bead of LATICRETE HYDRO BAN Adhesive & Sealant along the top edge of the tub or in the rabbet joint for the LATICRETE HYDRO BAN® Pre-Sloped Shower Pans and immediately install the LATICRETE HYDRO BAN Board.

2. To create the watertight system, the installation process will rely on the layering of components; start with the corners: Apply thin-set mortar (e.g. LATICRETE MULTIMAX™ LITE with a ¼”x 3/16” (6 mm x 5 mm) V-notched trowel. Press the LATICRETE HYDRO BAN pre-formed corner (e.g. LATICRETE HYDRO BAN Sheet Membrane Waterproofing Inside Corners or LATICRETE HYDRO BAN Sheet Membrane Waterproofing Outside Corners) firmly into the thin-set. Remove any trapped air and guarantee full adhesion to the material by spreading the thin-set from the inside of the corner out using a trowel or straightedge with rounded corners.

3. Continue with thin-set along the floor-to-wall transition from the corner outward for the first strip of LATICRETE HYDRO BAN Sheet Membrane Sealing Tape. Overlap the corners by a minimum of 2” (50 mm).

4. Lay the LATICRETE HYDRO BAN Sheet Membrane Sealing Tape and remove all air pockets and excess material as with the corner piece.

5. For any sections where two strips of LATICRETE HYDRO BAN Sheet Membrane Sealing Tape will be joined, be certain to overlap the material by 2” (50 mm).

6. Continue with these steps around the perimeter of the installation.

7. Treat the vertical corners for the HYDRO BAN Sheet Membrane Sealing Tape next in the same manner as the floor-to-wall transitions were installed. Overlap the corners by a minimum of 2” (50 mm).  Treat all LATICRETE HYDRO BAN Board joints in the same manner as the corners.

8. Treat pipe penetrations and mixing valves by applying thin-set mortar with a 1/4” x 3/16” (6 mm x 5 mm) V-notched trowel. Slide the appropriate LATICRETE HYDRO BAN Collar over the pipe or mixing valve and press firmly into the adhesive. The urethane rubber will seal around the pipe or mixing valve. Remove any trapped air and guarantee full adhesion to the material by spreading the adhesive from the inside out using a trowel or straightedge with rounded corners.

9. Washer and Fastener penetrations must be covered with LATICRETE HYDRO BAN Sheet Membrane Sealing Tape using a LATICRETE polymer fortified thin-set.

10. Important, there should not be excessive overlapping. For example, at the corner, the LATICRETE HYDRO BAN Sheet Membrane Sealing Tape that leaves the corner and protects the floor-to-wall transitions should overlap with the pre-formed corner piece, but not the pre-formed corner piece and the adjacent LATICRETE HYDRO BAN Sheet Membrane Sealing Tape.

- NOTE TO SPECIFIER: LATICRETE® HYDRO BAN® Board is two sizes; 3’ x 5’ (914 x 1,520mm) available in multiple thicknesses including: ¼” (6mm), 3/8” (9mm), ½” (12.7mm), 5/8” (16mm), 1” (25.4mm), 1 ½” (37.5mm), & 2” (50mm), and, 4’ x 8’ (1,220 x 2,440mm) available in ½” (12.7mm) thickness only.  LATICRETE HYDRO BAN Board to be used with LATICRETE HYDRO BAN Pre-Sloped Shower Pan to be ½” (12.7mm) thick.

NOTE TO SPECIFIER: LATICRETE HYDRO BAN Board provides an R value of 2.23 per ½” (12.7mm) of thickness.

Use the following LATICRETE System Materials:

LATICRETE® HYDRO BAN® Board

References:

LATICRETE Data Sheets: 040.0, 108.0

LATICRETE SDS: Adhesive & Sealant

Barrier Free Installation Manual: 012.5

- Waterproofing to Drains (Choose appropriate installation based on drain specified):

Clamping Ring Drains: When installing LATICRETE® HYDRO BAN® Sheet Membrane with a clamping ring type drains with weepers as per ASME A112.6.3, lay the LATICRETE HYDRO BAN Sheet Membrane over the top of the drain and cut an x where each bolt will penetrate the membrane. Cut a hole in the membrane to allow the drain grate to be threaded into the clamping ring. (Use of a fabric circle cutter is recommended). Install the LATICRETE HYDRO BAN Sheet Membrane, making sure to align the previously cut holes for the bolts and drain throat. Ensure that the weep holes are not blocked. Apply a bead of LATICRETE LATASIL™ to the clamping body just outside of the bolts, place clamping ring into position and tighten bolts. Check to make sure that weep holes are not plugged by any material.

HYDRO BAN Bonding Flange Drains: Follow the instructions in DS 035.0 for the installation of the LATICRETE HYDRO BAN Bonding Flange Drain in either a bonded or unbonded mortar bed. When the mortar is cured enough to walk on, prime the top of the LATICRETE HYDRO BAN Bonding Flange Drain, to the first 90 degree radius, and the adjusting ring with one coat of LATICRETE HYDRO BAN. Once the LATICRETE HYDRO BAN is dried to the touch the LATICRETE HYDRO BAN Sheet Membrane can be installed over it using a LATICRETE polymer fortified thin-set. Insure that the LATICRETE HYDRO BAN Sheet Membrane extends to the first 90° radius of the LATICRETE HYDRO BAN Bonding Flange Drain. Apply thin-set mortar (e.g. LATICRETE 254 Platinum, LATICRETE 254 Platinum Plus or LATICRETE MULTIMAX™ LITE) with a 1/4” x 3/16” (6mm x 5mm) V-notched trowel. Press the LATICRETE HYDRO BAN Sheet Membrane firmly into the adhesive. Remove any trapped air and guarantee full adhesion to the material by spreading the adhesive from the inside out using a trowel or straightedge with rounded corners. The adjusting ring is installed with a polymer fortified thin-set when installing the title in order to line up the grate with the tile.

HYDRO BAN Linear Drains: Follow the instructions in DS 034.0 for the installation of the HYDRO BAN Linear Drain in either a bonded or an unbonded mortar bed. When the mortar is cured enough to walk on, prime the top of the LATICRETE HYDRO BAN Linear Drain flange with LATICRETE HYDRO BAN, to the first 90 degree angle. Once the LATICRETE® HYDRO BAN® is dried to the touch the LATICRETE HYDRO BAN Sheet Membrane can be installed over it using LATICRETE 254 Platinum, LATICRETE 2254 Platinum Plus or LATICRETE MULTIMAX™ Lite. Apply thin-set mortar with a ¼”x3/16” (6 mm x 5 mm) V-notched trowel. Press the LATICRETE® HYDRO BAN® Sheet Membrane firmly into the adhesive. Remove any trapped air and guarantee full adhesion to the material by spreading the adhesive from the inside out using a trowel or straightedge with rounded corners.

NOTE: LATICRETE® HYDRO BAN® Sheet Membrane to be continuous over entire inside surface of steam room/steam shower and into the drain as stated below.  There can be no gaps, cuts or openings that would allow water/steam to escape into wall, floor or ceiling cavities.

Flood Testing: Allow LATICRETE 254 Platinum, LATICRETE 254 Platinum Plus or LATICRETE MULTIMAX™ LITE to cure fully before flood testing, a minimum of 24 hours after final cure at 70°F (21°C) and 50% RH. Cold and/or wet conditions will require a longer curing time.

Control Joints: Ceramic tile, porcelain tile, stone and mosaic installations must include sealant-filled joints between the ceramic tile, stone or brick, which is over any control joints in the substrate. However, the sealant-filled joints can be offset horizontally by as much as one tile width from the substrate control joint location to coincide with the grout joint pattern.

Movement Joints: Ceramic tile, porcelain tile, stone and mosaic installations must include expansion joints at coves, corners, other changes in substrate plane and over any expansion joints in the substrate. Expansion joints in ceramic tile, porcelain tile and stone are also required at perimeters, at restraining surfaces, at penetrations and at the intervals described in the Tile Council of North America, Inc. (TCNA) Handbook Installation Method EJ171. Use LATICRETE LATASIL™, LATICRETE LATASIL 9118 Primer and backer rod.  Loop LATICRETE HYDRO BAN Sheet Membrane into all slip and movement joints to allow for excessive movement in these areas.

Use the following LATICRETE System Materials:

LATICRETE® HYDRO BAN® Sheet Membrane

References:

LATICRETE Data Sheets: 041.0; 034.0; 035.0; 328.0; 663.0

LATICRETE SDS: MULTIMAX LITE; HYDRO BAN

Health Product Declaration: MULTIMAX LITE (Grey) , MULTIMAX LITE (White)

Product Specific (Type III) Environmental Product Declaration: Mortar EPD

UL GREENGUARD GOLD Certificate: MULTIMAX LITE; HYDRO BAN

- Bonded Thick Bed Method: Verify 1” (25mm) nominal bed thickness has been allowed.  Apply LATICRETE 254 Platinum with flat trowel as a slurry bond coat approximately 1/16” (1. 5mm) thick over clean concrete slab in compliance with current revision of ANSI A108.1A (2.2 and 5.2).  Place LATICRETE 3701 Fortified Mortar mixed with water over slurry bond coat while LATICRETE 254 Platinum slurry bond coat is wet and tacky.  Omit reinforcing wire fabric and fully compact bed by tamping.  Spread LATICRETE 254 Platinum with flat trowel over surface of "green"/fresh mortar bed as a slurry bond coat approximately 1/16” (1.5mm) thick.  Apply LATICRETE 254 Platinum slurry bond coat to back of ceramic tile, mosaic, paver, brick, stone, trim unit, or threshold and place each piece/sheet while slurry bond coats are wet and tacky.  Beat with a hardwood block or rubber mallet to level/imbed pieces before mortar bed takes initial set.  Clean excess mortar/adhesive from finished surfaces.  For installation of tile, brick, or stone over cured (pre-floated) latex-portland cement thick bed mortar, follow Thin Bed Mortar (§3.4F 1) or Large, Heavy Tile (Medium Bed) Method (§3.4F 2). Ensure ¼” (6mm) gap between mortar bed edge and wall(s) to allow for movement.

Use the following LATICRETE System Materials:

LATICRETE® 3701 Fortified Mortar

LATICRETE 254 Platinum *

References:

LATICRETE Data Sheets: 100.0; 677.0

LATICRETE SDS: 3701 FMB; 254

Health Product Declarations: 3701FMB HPD,  254 HPD (Grey), 254 Platinum (White)

Product Specific (Type III) Environmental Product Declaration: Mortar EPD

UL GREENGUARD GOLD Certificates:  3701FMB; 254 Platinum

LATICRETE Technical Data Sheets: 106, 114, 118, 128, 143, 154, 204, 233, 251

* NOTE to Specifier: LATICRETE® 254 Platinum Plus can replace LATICRETE 254 Platinum as the slurry bond coat.

- Secondary Waterproofing / Crack Isolation Membrane installed over cured mortar bed on the floor surfaces and turned up the vertical surfaces at least 6” (150mm) onto the existing waterproofing membrane.  Loop membrane into all slip and movement joints to allow for movement in these areas.

NOTE TO SPECIFIER:  Adhesives/mastics, mortars and grouts for ceramic tile, mosaics, pavers, thin brick, masonry veneer, and stone are not replacements for waterproofing membranes and will not prevent water penetration into occupied or storage spaces below.

Install the waterproofing membrane in compliance with current revisions of ANSI A108.01 (2.7 Waterproofing) and ANSI A108.13.  Review the installation and plan the application sequence.  Pre-cut LATICRETE® Waterproofing/Anti-Fracture Fabric (if required), allowing 2” (50mm) for overlap at ends and sides to fit the areas as required.  Roll up the pieces for easy handling and placement.

Pre-Treat Cracks and Joints - Fill all substrate cracks, cold joints, and control joints to a smooth finish using a LATICRETE Latex Fortified Thin-Set. Alternatively, a liberal coat** of LATICRETE HYDRO BAN® XP applied with a paint brush or trowel may be used to fill in non-structural joints and cracks. Apply a liberal coat** of LATICRETE HYDRO BAN XP approximately 8" (200 mm) wide over substrate cracks, cold joints, and control joints using a paint brush or roller (heavy napped roller cover). 6" (150 mm) LATICRETE Waterproofing/Anti-Fracture Fabric can be used to pretreat cracks, joints, curves, corners, drains and penetrations with LATICRETE HYDRO BAN XP.

Pre-Treat Coves and Floor/Wall Intersections - Fill all substrate coves and floor/wall transitions to a smooth finish and changes in plane using a LATICRETE latex-fortified thin-set.  Alternatively, a liberal coat** of LATICRETE HYDRO BAN XP applied with a paint brush or trowel may be used to fill in cove joints and floor/wall transitions <1/8” (3mm) in width.  Apply a liberal coat** of LATICRETE HYDRO BAN XP approximately 8” (200mm) wide over substrate cracks, cold joints, and control joints using a paint brush or roller (heavy napped roller cover).

Pre-Treat Drains - Drains must be of the clamping ring type, with weepers as per ASME A112.6.3.  Apply a liberal coat** of LATICRETE HYDRO BAN XP around and over the

bottom half of drain clamping ring.  Cover with a second liberal coat of LATICRETE® HYDRO BAN® XP.  When dry, apply a bead of LATICRETE LATASIL™ where the LATICRETE HYDRO BAN XP meets the drain throat.  Install the top half of drain clamping ring.

Pre-Treat Penetrations - Allow for a minimum 1/8” (3mm) space between drains, pipes, lights, or other penetrations and surrounding ceramic tile, stone or brick.  Pack any gaps around pipes, lights or other penetrations with a LATICRETE latex-fortified thin-set.  Apply a liberal coat** of LATICRETE HYDRO BAN XP around penetration opening.  Cover the first coat with a second liberal coat** of LATICRETE® HYDRO BAN® XP.  Bring LATICRETE HYDRO BAN XP up to level of tile or stone.  When LATICRETE HYDRO BAN XP has dried to the touch seal with LATICRETE LATASIL.

** Each wet coat should be 15 – 22 mils (0.015 - 0.022” or 0.4 - 0.6mm) thick; consumption per coat is approximately 0.01 gal/ft2 (approx. 0.4 L/m2); coverage is approximately 100 ft2 /gal (approx. 2.5 m2/ L).  The combined dry coat thickness should be 20 – 30 mils (0.02 – 0.03” or 0.5 – 0.8mm) thick. LATICRETE® Waterproofing/Anti-Fracture Fabric can be used to pre-treat cracks, joints, curves, corners, drains, and penetrations with LATICRETE HYDRO BAN® XP.

Main Application

Allow any pre-treated areas to dry to the touch. Apply a liberal coat** of LATICRETE HYDRO BAN XP with brush or roller over substrate including pretreated areas. Apply another liberal coat** of LATICRETE HYDRO BAN XP over the first coat of LATICRETE HYDRO BAN XP. Let topcoat dry to the touch, approximately 1–2 hours at 70°F (21°C) and 50% RH. When last coat has dried to the touch, inspect final surface for pinholes, voids, thin spots, or other defects. LATICRETE HYDRO BAN XP will turn a darker green when it's dry to touch. Use additional LATICRETE HYDRO BAN XP to seal defects.

Movement Joints

See LATICRETE HYDRO BAN XP Installation Instructions DS 10003.

Note: Apply a liberal coat** of LATICRETE HYDRO BAN XP, approximately 8" (200 mm) wide over the areas. Then embed and loop the 6" (150 mm) wide Waterproofing/Anti-Fracture Fabric and allow to bleed through. Then top coat with a second liberal coat** of LATICRETE HYDRO BAN XP.

Protection - Provide protection for newly installed membrane, even if covered with a thin-bed ceramic tile, stone, masonry veneer, or brick installation against exposure to rain or other water for a minimum of 2 hours after final cure at 70°F (21°C) and 50% RH.  For temperatures between 35°F – 69°F (2 – 21°C) allow a minimum 24-hour cure period.

Flood Testing - Allow membrane to cure fully before flood testing, typically 2 hours after final cure at 70°F (21°C) and 50% RH. Cold and/or wet conditions will require a longer curing time. For temperatures 35°F – 69°F (2 – 21°C) allow 24 hours after final cure prior to flood testing.  Please refer to LATICRETE TDS 169 “Flood Testing Procedures”, available at https://laticrete.com for flood testing requirements and procedures.

Installing Finishes

Once LATICRETE HYDRO BAN XP has dried to the touch, ceramic tile, stone or brick may be installed by the thin bed method with a LATICRETE Latex Thin-Set Mortar. Allow LATICRETE HYDRO BAN XP to cure 2 hours at 70°F (21°C) and 50% RH before covering with, thick bed mortar, epoxy adhesives, terrazzo, or moisture sensitive resilient or wood flooring. Do not use solvent-based adhesives directly on LATICRETE® HYDRO BAN® XP.

Drains & Penetrations

Use LATICRETE® LATASIL™ and foam backer rod to seal space between drain or penetration and finish. Do not use a grout or joint filler mortar.

Control Joints

Ceramic tile, stone and brick installations must include sealant filled joints over any control joints in the substrate. However, the sealant filled joints can be offset horizontally by as much as one tile width from the substrate control joint location to coincide with the grout joint pattern.

Movement Joints

Ceramic tile, stone and thin brick installations must include expansion at coves, corners, other changes in substrate plane and over any expansion joints in the substrate. Expansion joints in ceramic tile, stone or brickwork are also required at perimeters, at restraining surfaces, at penetrations and at the intervals described in the Tile Council of North America, Inc. (TCNA) Handbook Installation Method EJ-171.

** Each wet coat should be 15 – 22 mils (0.015 - 0.022” or 0.4 - 0.6mm) thick; consumption per coat is approximately 0.01 gal/ft2 (approx. 0.4 L/m2); coverage is approximately 100 ft2 /gal (approx. 2.5 m2/ L).  The combined dry coat thickness should be 20 – 30 mils (0.02 – 0.03” or 0.5 – 0.8mm) thick. LATICRETE® Waterproofing/Anti-Fracture Fabric can be used to pre-treat cracks, joints, curves, corners, drains, and penetrations with LATICRETE HYDRO BAN® XP.

Use the following LATICRETE System Materials:

LATICRETE® HYDRO BAN® XP

References:

LATICRETE Detail Drawings: WP300

LATICRETE Data Sheets: 36642.0, 10003

LATICRETE SDS: HYDRO BAN XP

Health Product Declaration: HYDRO BAN XP HPD

UL GREENGUARD GOLD Certificate: HYDRO BAN XP

LATICRETE Technical Data Sheets: 166, 169, 183, 203, 251

- F.	NOTE TO SPECIFIER: select one of following tile adhesive mortars based on application method:

1.    Thin Bed Method:  Install latex portland cement mortar in compliance with current revisions of ANSI A108.02 (3.11), A108.1B and ANSI A108.5.  Use the appropriate trowel notch size to ensure proper bedding of the tile, brick or stone selected.  Work the latex portland cement mortar into good contact with the substrate and comb with notched side of trowel.  Spread only as much latex portland cement mortar as can be covered while the mortar surface is still wet and tacky.   When installing large format (>8” x 8” [200mm x 200mm]) tile/stone, rib/button/lug back tiles, pavers, or sheet mounted ceramics/mosaics, spread latex portland cement mortar onto the back of (i.e. ‘back-butter’) each piece/sheet in addition to troweling latex portland cement mortar over the substrate.  Beat each piece/sheet into the latex portland cement mortar with a beating block or rubber mallet to insure full bedding and flatness. Allow installation to set until firm. Clean excess latex portland cement mortar from tile or stone face and joints between pieces.

Use the following LATICRETE System Materials:

LATICRETE® 254 Platinum

References:

LATICRETE Data Sheet: 677.0

LATICRETE SDS: 254

Health Product Declaration: 254 HPD

Product Specific (Type III) Environmental Product Declaration: Mortar EPD

UL GREENGUARD GOLD Certificate: 254

LATICRETE Technical Data Sheets: 105, 129, 209

or,

LATICRETE 254 Platinum Plus

References:

LATICRETE Data Sheets: 65329

LATICRETE SDS: 254 Platinum Plus

Health Product Declarations: 254 Platinum Plus HPD (Grey), 254 Platinum Plus HPD (White)

Product Specific (Type III) Environmental Product Declaration: Mortar EPD

UL GREENGUARD GOLD Certificates:  254 Platinum Plus

LATICRETE Technical Data Sheets: 105, 129, 209

or,

2.   Large, Heavy Tile (Medium Bed) Mortar Method:  Install latex portland cement mortar in compliance with current revisions of ANSI A108.02 (3.11), A108.1B and ANSI A108.5.  Use the appropriate trowel notch size to ensure proper bedding of the tile, brick or stone selected.  Work the latex portland cement mortar into good contact with the substrate and comb with notched side of trowel.  Spread only as much latex portland cement mortar as can be covered while the mortar surface is still wet and tacky.  When installing large format (>8” x 8” [200mm x 200mm]) tile/stone, rib/button/lug back tiles, pavers, or sheet mounted ceramics/mosaics, spread latex portland cement mortar onto the back of (i.e. ‘back-butter’) each piece/sheet in addition to troweling latex portland cement mortar over the substrate.  Beat each piece/sheet into the latex portland cement mortar with a beating block or rubber mallet to insure full bedding and flatness. Allow installation to set until firm. Clean excess latex portland cement mortar from tile or stone face and joints between pieces.

Use the following LATICRETE System Materials:

LATICRETE MULTIMAX™ LITE

References:

LATICRETE Data Sheet: 328.0

LATICRETE SDS: MULTIMAX LITE

Health Product Declaration: MULTIMAX LITE (Grey) , MULTIMAX LITE (White)

Product Specific (Type III) Environmental Product Declaration: Mortar EPD

UL GREENGUARD GOLD Certificate: MULTIMAX LITE

LATICRETE Technical Data Sheets: 105, 118, 126, 129, 209, 233, 251

F.	Grouting or Pointing:

- NOTE TO SPECIFIER: select one of following and specify color for each type/color of ceramic tile, mosaic, paver, trim unit:

1.  Chemical Resistant, Water Cleanable Tile-Grouting Epoxy (ANSI A118.3):  Follow manufacturers’ recommendations for minimum cure time prior to grouting.  Store liquid components of LATICRETE® SPECTRALOCK® PRO Premium Grout† for 24 hours @ 70-80˚F (21-27˚C) prior to use to facilitate mixing and application. Substrate temperature must be 40-95˚F (4-35˚C).  Verify joints are free of dirt, debris or grout spacers. Sponge or wipe dust/dirt off tile faces and remove water standing in joints.  Apply grout release to face of absorptive, abrasive, non-slip or rough textured ceramic tile, pavers, bricks, stone, or trim units that are not hot paraffin coated to facilitate cleaning.  Cut open pouch and pour LATICRETE® SPECTRALOCK® PRO Premium Grout Part A Liquid into a clean mixing pail.  Then open pouch and pour LATICRETE SPECTRALOCK PRO Premium Grout Part B Liquid into the mixing pail.  Mix by hand or with a slow speed (<300 rpm) mixer until the two liquids are well blended.  Then, while mixing, add LATICRETE SPECTRALOCK Grout Part C Powder and blend until uniform.  For narrow joints, it is acceptable to leave out up to 10% of the LATICRETE SPECTRALOCK Grout Part C Powder to produce a more fluid mix. Install LATICRETE SPECTRALOCK PRO Premium Grout in compliance with current revisions of ANSI A108.02 (3.13) and ANSI A108.6 (3.0 - 4.0).  Spread using a sharp edged, firm rubber float and work grout into joints.  Using strokes diagonal (at 45˚ angle) to the grout lines, pack joints full and free of voids/pits.  Then hold float face at a 90˚ angle to grouted surface and use float edge to "squeegee" off excess grout, stroking diagonally to avoid pulling grout out of filled joints.  Once excess grout is removed, a thin film/haze will be left.  Initial cleaning of the remaining film/haze can begin approximately 20 minutes after grouting (wait longer when temperatures are cooler).  Begin by mixing one cleaning additive packet with 2 gallons (7.6 L) of clean water in a clean bucket to make cleaning solution. Dip a clean sponge into the bucket and then wring out cleaning solution until sponge is damp. Using a circular motion, lightly scrub grouted surfaces with the damp sponge to loosen grout film/haze.  Then drag sponge diagonally over the scrubbed surfaces to remove froth.  Rinse sponge frequently and change cleaning solution at least every 50 ft2 (4.7m2).  Discard sponges as they become "gummy" with residue.  Check work as you clean and repair any low spots with additional grout. One (1) hour after finishing first cleaning, clean the same area again following the same procedure but utilizing a clean white scrub pad and fresh cleaning solution. Rinse scrub pad frequently.  Drag a clean sponge diagonally over the scrubbed surfaces to remove froth.  Use each side of sponge only once before rinsing and change cleaning solution at least every 50 ft2 (4.7m2).  Allow cleaned areas to dry and inspect tile/stone surface.  For persistent grout film/haze (within 24 hours), repeat scrubbing procedure with undiluted white vinegar and clean pad.  Rinse with clean water and allow surface to dry.  Inspect grout joint for pinholes/voids and repair them with freshly mixed LATICRETE® SPECTRALOCK® PRO Premium Grout†.  Cautions: Do not use undiluted white vinegar on polished marble or limestone unless a test spot in an inconspicuous area indicates no change in finish appearance; do not use acid cleaners on epoxy grout less than 7 days old.

Use the following LATICRETE System Materials:

LATICRETE® SPECTRALOCK® PRO Premium Grout

References:

LATICRETE Data Sheets: 681.0, 681.5

LATICRETE SDS: Premium Part A, Premium Part B, Part C Powder, Cleaning Additive

Health Product Declaration: PRO Premium HPD

UL GREENGUARD GOLD Certificate: PRO Premium

LATICRETE Technical Data Sheets: 111, 198, 216, 251, 400

2. Polymer Fortified Cement Grout (ANSI A118.7):   Allow ceramic tile, mosaics, pavers, brick, or stone installation to cure a minimum of 24 hours @ 70˚F (21˚C).  Verify grout joints are free of dirt, debris or tile spacers. Sponge or wipe dust/dirt off veneer face and remove any water standing in joints.  Apply grout release to face of absorptive, abrasive, non-slip or rough textured ceramic tile, pavers, bricks, or trim units that are not hot paraffin coated to facilitate cleaning.  Surface temperature must be between 40 to 90˚F (4 to 32˚C). Use approximately 2 – 2.25 quarts (1.9 L – 2.1 L) of clean potable water for 2 LATICRETE PERMACOLOR® Select Color Packs and 25 lbs. (11.4 kg) of LATICRETE PERMACOLOR Select Base. Do not use with any latex additive. Place water in a clean mixing container. If using the 25 lb. (11.4 kg) bag, remove LATICRETE PERMACOLOR Select Color Packs from the cardboard container as well as the protective plastic sleeve. The internal bag is a water-dispersible pack – drop both color packs directly to water in clean mixing container. Mix with a drill mixer until pigment is dispersed evenly in container and the dispersible pack is no longer visible. Add LATICRETE PERMACOLOR Select Base. Mix with a slow speed drill mixer (300 rpm) for 1 minute. Wait for 5 minutes and remix with drill for 1 minute. If using the 12.5 lb. (5.7 kg) bag, drop only one color pack into 1 – 1.1 quarts (0.8 L – 1.0 L) of clean water.  Install latex fortified cement grout in compliance with current revisions of ANSI A108.1A (7.0 Grouting of tile), ANSI A108.02 (4.5 Cleaning tile) and ANSI A108.10.  Clean tile surface with a damp sponge. Spread with a sharp, firm, rubber grout float or wall float for narrow wall joints. To remove excess grout hold the float at a 90° angle and pull it at a 45° angle diagonally across the joints to avoid pulling out the material.  Wait 35 – 40 minutes at 70°F (21°C). For wider joints or cooler temperatures, wait longer (25 – 30 minutes) Begin initial cleaning by lightly wiping down entire area to be cleaned with a damp sponge. Wash with a damp sponge (not wet). Work diagonally to the joints. Allow to dry 3 hours at 70°F (21°C). For the second cleaning, use a damp sponge or dry cloth to remove remaining grout haze. Buff surface of grout with clean coarse cloth.  Inspect joint for pinholes/voids and repair them with freshly mixed grout. Within 24 hours, check for remaining haze and remove it with warm soapy water and a nylon scrub pad, using a circular motion, to lightly scrub surfaces and dissolve haze/film.  Do not use acid cleaners on latex portland cement grout less than 10 days old.

NOTE: Use caution when polishing soft glazed tile or polished stone. If grout is to be sealed, LATICRETE generally recommends waiting a minimum of a 72 hours at 70°F (21°C) prior to sealing LATICRETE® PERMACOLOR® Select^ with a STONETECH® sealer. However, we suggest deferring to the written recommendations of the STONETECH sealer to make the final determination, as certain sealers may require the cement grout to cure for an extended period.

- NOTE TO SPECIFIER: select one of following and specify color for each type/color of ceramic tile, mosaic, paver, trim unit:

  - latex-portland cement sanded floor grout for joint widths ≥1/16” (1.5mm) and ≤1/2” (12mm);

  - latex-portland cement unsanded grout for soft glazed tiles and soft/polished stone with joints widths ≤1/8” (3mm).

Use the following LATICRETE System Materials:

LATICRETE® PERMACOLOR® Select

References:

LATICRETE Data Sheets: 281.0

LATICRETE SDS: 2600, Color Kit

Health Product Declaration: Select Powder HPD, Select Color Kit HPD

Environmental Product Declaration: Grout EPD

UL GREENGUARD Gold Certificate:  2600

LATICRETE Technical Data Sheets: 201, 251, 400

G.   Expansion and Control Joints:  Provide control or expansion joints as located in contract drawings and in full conformity, especially in width and depth, with architectural details.

- Substrate joints must carry through, full width, to surface of tile, brick, masonry veneer, or stone.

- Install expansion joints in tile, brick, masonry veneer, or stone work over construction/cold joints or control joints in substrates.

- Install expansion joints where ceramic tile, porcelain tile or stone abut restraining surfaces (such as perimeter walls, curbs, columns), changes in plane and corners.

- Joint width and spacing depends on application - follow Tile Council of North America “Handbook for Ceramic, Glass, and Stone Tile Installation” Detail "EJ-171 Expansion Joints" or consult sealant manufacturer for recommendation based on project parameters.

- Joint width: ≥ ⅛” (3mm) and ≤ 1” (25mm).

- Joint width: depth ~2:1 but joint depth must be ≥ ⅛” (3mm) and ≤ ½” (12mm).

- Layout (field defined by joints): 1:1 length: width is optimum but must be ≤ 2:1. Remove all contaminants and foreign material from joint spaces/surfaces, such as dirt, dust, oil, water, frost, setting/grouting materials, sealers, and old sealant/backer.  Use LATICRETE® LATASIL™ 9118 Primer for underwater and permanent wet area applications, or for porous stone (e.g. limestone, sandstone etc…) installations.  Install appropriate backing material (e.g. closed cell backer rod) based on expansion joint design and as specified in §07 92 00.  Apply masking tape to face of tile, brick or stone veneer.  Use caulking gun, or other applicator, to fill joints with sealant.  Within 5-10 minutes of filling joint, ‘tool’ sealant surface to a smooth finish.  Remove masking tape immediately after tooling joint.  Wipe smears or excess sealant off the face of non-glazed tile, brick, stone, or other absorptive surfaces immediately.

Use the following LATICRETE System Materials:

LATICRETE® LATASIL™

LATICRETE LATASIL 9118 Primer

References:

LATICRETE Detail Drawings: WP300, WP301, WP302, WP303, EJ-01, EJ-02, EJ-03, EJ-04, EJ-05, EJ-06, EJ-07, EJ-08, EJ-09, EJ-10, EJ-11, EJ-12, EJ-13, EJ-14  (Sealant treatments only)

LATICRETE Data Sheets: 6200.1,  6528.1

LATICRETE SDS: LATASIL, Primer

VOC Emission Testing: Certificate, Report

LATICRETE Technical Data Sheets: 211, 251, 252

H.   Adjusting:  Correction of defective work for a period of one (1) year following substantial completion, return to job and correct all defective work.  Defective work includes, without limitation, tiles broken in normal abuse due to deficiencies in setting bed, loose tiles or grout, and all other defects that may develop as a result of poor workmanship.

3.5	CLEANING

Clean excess mortar/epoxy from veneer surfaces with water before they harden and as work progresses.  Do not contaminate open grout/caulk joints while cleaning. Sponge and wash veneers diagonally across joints. Do not use acids for cleaning. Polish with clean dry cloth. Remove surplus materials and leave premises broom clean.

3.6	PROTECTION

A.   Owner/specifier is responsible for protecting the tile work from damage, including sufficient time for installed materials to cure properly. Protection of installation may be required to prevent premature exposure of setting materials to moisture or rain.

- Protect finished installation under provisions of §01 50 00 and §01 56 00. To avoid damage to finished tile work, schedule floor installations to begin only after all structural work, building enclosure, and overhead finishing work are completed. Keep all traffic off finished tile floors until they have fully cured. Builder shall provide up to ¾” (19mm) thick

plywood or OSB protection over non-staining Kraft® paper to protect floors after installation materials have cured. Covering the floor with polyethylene or plywood in direct contact with the floor may adversely affect the curing process of grout and latex/polymer fortified portland cement mortar. Keep traffic off horizontal portland cement thick bed mortar installations for at least 72 hours @ 70˚F (21˚C).

C.   Keep floors installed with epoxy adhesive closed to foot traffic for 24 hours @ 70˚F (21˚C), and to heavy traffic for 48 hours @ 70˚F (21˚C) unless instructed differently by manufacturer. Use kneeling boards, or equivalent, to walk/work on newly tiled floors. Cure tile work in swimming pools, fountains and steam room applications for 10 days @ 70˚F (21˚C) for epoxy based grout and 14 days @ 70˚F (21˚C) for latex portland cement based grout before flood testing or turning on steam generators. Extend period of protection of tile work at lower temperatures, below 60˚F (15˚C), and at high relative humidity (>70% RH) due to retarded set times of mortar/adhesives. Replace or restore work of other trades damaged or soiled by work under this section.

PART 4 – HEALTH AND SAFETY

The use of personal protection such as rubber gloves, suitable dust masks, safety glasses and industrial clothing is highly recommended. Discarded packaging, product wash and wastewater should be disposed of as per local, state or federal regulations.

"As a professional courtesy, LATICRETE offers technical services free of charge. The user maintains all responsibility for verifying the applicability and suitability of the technical service or information provided."

The right to copy, distribute and utilize for commercial purposes is granted exclusively to architects, engineers, and specification writers.  Execution Statements are subject to change without notice.  For latest revision, check our website @ https://laticrete.com

ES-SR614         R  01 May 2024

†  United States Patent No.: 6,881,768 (and other Patents)

All references are the intellectual property of their respective owners:

TCNA Handbook for Ceramic, Glass, and Stone Tile Installation. Tile Council of North America, Inc. Anderson, SC, 2021.

American National Standard Specifications for Installation of Ceramic Tile. Tile Council of North America, Inc. Anderson, SC, 2021.

Annual Book of ASTM Standards. American Society for Testing and Materials. West Conshohocken, PA, 2001.

American National Standard Specifications for Ceramic Tile (ANSI A137.1). Tile Council of North America, Inc. Anderson, SC 2021.

American National Standard Specifications for Glass Tile (ANSI A137.2). Tile Council of North America, Inc. Anderson, SC, 2019.

American National Standard Specifications for Gauged Porcelain Tile and Gauged Porcelain Tile Panels/Slabs (ANSI A137.3). Tile Council of North America, Inc. Anderson, SC, 2020.

ISO 13007 Ceramic Tiles – Grouts and Adhesives, International Organization for Standardization (ISO), Geneva, Switzerland, 2004.

Floor and Trench Drains - ASME A112.6.3. American Society of Mechanical Engineers. New York, NY, 2001 (R 2007).

International Building Code, International Code Council. Country Club Hills, IL, 2018.

International Residential Code for One- and Two-Family Dwellings, International Code Council. Country Club Hills, IL, 2018.

LEED Reference Guide for Green Building Design and Construction v4. U.S Green Building Council. Washington, D.C., 2013.

LEED Schools Reference Guide. U.S. Green Building Council. Washington D.C., 2007.

Lightweight Steel Framing Design Manual. Canadian Sheet Steel Building Institute. Cambridge, ON, Canada, 2006.

North American Specification for the Design of Cold-Formed Steel Structural Members. American Iron and Steel Institute. Washington D.C., 2007.

ICBO ER-4943P Product Technical Information. Steel Stud Manufacturers Association. Chicago, IL, 2001.

Lightweight Steel Framing Systems Manual. Metal Lath/Steel Framing Association Division. Glen Ellyn, IL.